 SEQ CHAPTER \h \r 1
SECTION 09 21 16.23

GYPSUM BOARD SHAFT WALL ASSEMBLIES







THIS SECTION IS WRITTEN IN CSI 3-PART FORMAT AND IN CSI PAGE FORMAT; THE PROJECT NAME/NUMBER/DATE AND SECTION TITLE IN THE FOOTER ARE OPTIONAL. NOTES TO THE SPECIFIER, SUCH AS THIS, MUST BE DELETED FROM THE FINAL SPECIFICATION.

IT IS ASSUMED THAT THE GENERAL CONDITIONS BEING USED ARE AIA A201-1997.

PART
1
GENERAL

1.01
SUMMARY







IF THE PROJECT INCLUDES ALLOWANCES OR ALTERNATES OR UNIT PRICES, RETAIN PARAGRAPHS BELOW AND COORDINATE WITH DIVISION 01.


A.
Allowances:


B.
Unit Prices:


C.
Alternates:

1.02
REFERENCES


A.
ASTM International (ASTM):



1.
ASTM C475 Standard Specification for Joint Compound and Joint Tape for Finishing Gypsum Board.



2.
ASTM C518 Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus.



3.
ASTM C645 Standard Specification for Nonstructural Steel Framing Members.



4.
ASTM C840 Standard Specification for Application and Finishing of Gypsum Board.



5.
ASTM C1002 Standard Specification for Steel Self-Piercing Tapping Screws for the Application of Gypsum Panel Products or Metal Plaster Bases to Wood Studs or Steel Studs.



6.
ASTM C1047 Standard Specification for Accessories for Gypsum Wallboard and Gypsum Veneer Base.



7.
ASTM C1396 Standard Specification for Gypsum Board.


8.
ASTM C1658 Standard Specification for Glass Mat Gypsum Panels.


9.
ASTM D3273 Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber.



10.
ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials.



11.
ASTM E488 Standard Test Methods for Strength of Anchors in Concrete and Masonry Elements.



12.
ASTM E1190 Standard Test Methods for Strength of Power-Actuated Fasteners Installed in Structural Members.


B.
Gypsum Association (GA):



1.
GA-214 Levels of Gypsum Board Finish.



2.
GA-216 Application and Finishing of Gypsum Board.

1.03
SUBMITTALS


A.
Product Data: Manufacturer’s specifications and installation instructions for each product specified.
1.04
QUALITY ASSURANCE







RETAIN BELOW IF REQUIRED, REVISE LIMITS IF REQUIRED.


A.
Regulatory Requirements: Provide products that comply with the following limits for surface burning characteristics when tested per ASTM E84:



1.
Flame spread: 25, maximum.



2.
Smoke developed: 450, maximum.
1.05
WARRANTY


A.
Provide products that offer twelve months of coverage against in-place exposure damage (delamination, deterioration and decay).


B.
Manufacturer’s Warranty: Five years against manufacturing defects.






THIS GUIDE SPEC WAS WRITTEN TO PROVIDE THREE EDITING OPTIONS: 1) PROPRIETARY, 2) GENERIC, OR 3) A COMBINATION OF THE TWO.

PART
2
PRODUCTS

IF PROPRIETARY PRODUCT NAMES ARE INCLUDED IN THE “MATERIALS” ARTICLE BELOW, DELETE THIS ARTICLE ALTOGETHER. IF A PROPRIETARY SPECIFICATION IS REQUIRED, RETAIN THIS ARTICLE AND DELETE THE “MATERIALS” ARTICLE.

2.01
MANUFACTURERS

EDIT LISTS BELOW TO CONFORM TO PROJECT REQUIREMENTS. IF OTHER MANUFACTURERS ARE BEING ADDED TO THIS SECTION, ADD LISTINGS OF THEIR PROPRIETARY PRODUCT NAMES.


A.
Metal Framing:



1.
Dietrich Metal Framing.



2.
Marino\WARE.



3.
Western Metal Lath.


B.
Gypsum Board:



1.
Georgia-Pacific Gypsum LLC:



a.
Shaftliner Board: DensGlass Ultra Shaftliner.




b.
Fire-Rated Paper Faced Gypsum Board: 1/2" ToughRock Fireguard C.




c.
Fire-Rated Paper Faced Gypsum Board: 1/2" ToughRock Fireguard.




d.
Fire-Rated Fiberglass-Mat Faced Gypsum Board: 1/2" DensArmor Plus Fireguard C.




e.
Fire-Rated Fiberglass-Mat Faced Gypsum Board: 5/8" DensArmor Plus Fireguard.



2.



3.

THIS ARTICLE INCLUDES GENERIC DESCRIPTIONS OF GYPSUM BOARD SHAFTWALL PANELS; THE NAMES OF THE CORRESPONDING GEORGIA-PACIFIC GYPSUM PRODUCTS ARE INCLUDED AS ACCEPTABLE PRODUCTS. IF THIS SECTION IS BEING EDITED TO BE GENERIC, THESE PRODUCT NAMES SHOULD BE DELETED.

IF OTHER MANUFACTURERS ARE BEING ADDED TO THIS SECTION, 1) ADD THE PROPRIETARY PRODUCT NAMES OF THOSE MANUFACTURERS, OR 2) IF PROPRIETARY NAMES ARE LISTED IN THE “MANUFACTURERS” ARTICLE ABOVE, DELETE THEM FROM THIS ARTICLE ALTOGETHER.

2.02
MATERIALS


A.
Metal Framing:



1.
J Track: ASTM C645, galvanized steel.







AVAILABLE WIDTHS ARE 2-1/2, 4, AND 6 INCHES, IF NOT INDICATED ON THE DRAWINGS, INSERT REQUIRED WIDTH BELOW.




a.
Width: As indicated on the drawings.




b.
Gauge: 20 at elevator doors and masonry cavities, 25 at all other locations.


2.
C-T, C-H, or I Studs: ASTM C645, galvanized steel.







AVAILABLE WIDTHS ARE 2-1/2, 4, AND 6 INCHES, IF NOT INDICATED ON THE DRAWINGS, INSERT REQUIRED WIDTH BELOW.




a.
Width: As indicated on the drawings.







20 GAUGE IS ALSO AVAILABLE, REVISE BELOW AS REQUIRED.




b.
Gauge: 25.







EDIT LIST BELOW TO CONFORM TO PROJECT REQUIREMENTS.

A.
Gypsum Board:







PARAGRAPH BELOW IS DENSGLASS ULTRA SHAFTLINER.


1.
Shaftliner Board:




a.
Material Standard: Comply with applicable sections of ASTM C1396 and ASTM C1658.




b.
Thickness: 1 inch.




c.
Width: 2 feet.




d.
Length: 8 feet.




e.
Weight: 4000 pounds per M square feet.




f.
Edges: Double bevel.




g.
R-Value (ASTM C518): 0.67.




h.
Acceptable Products:





1)
DensGlass Ultra Shaftliner.





2)





3)







PARAGRAPH BELOW IS 1/2 INCH TOUGHROCK FIREGUARD C.



2.
Fire-Rated Paper Faced Gypsum Board:




a.
Thickness: 1/2 inch.




b.
Width: 4 feet.




c.
Length: 8 feet.




d.
Weight: 1850 pounds per M square feet.




e.
Edges: [Tapered] [Square] [Rounded].




f.
Flexural Strength, Parallel (ASTM C1396): 40 pounds per square inch.




g.
Flexural Strength, Perpendicular (ASTM C1396): 110 pounds per square inch.




h.
R-Value (ASTM C518): 0.45.




i.
Nail Pull Resistance (ASTM C1396): Not less than 80 lbf.




j.
Hardness, Core, Edges, and Ends (ASTM C1396): Greater than 15 lbf.




k.
Acceptable Products:





1)
1/2" ToughRock Fireguard C.





2)





3)







PARAGRAPH BELOW IS 5/8 INCH TOUGHROCK FIREGUARD C.



2.
Fire-Rated Paper Faced Gypsum Board:




a.
Thickness: 5/8 inch.




b.
Width: 4 feet.




c.
Length: 8 feet.




d.
Weight: 2200 pounds per M square feet.




e.
Edges: [Tapered] [Square] [Rounded].




f.
Flexural Strength, Parallel (ASTM C1396): 50 pounds per square inch.




g.
Flexural Strength, Perpendicular (ASTM C1396): 150 pounds per square inch.




h.
R-Value (ASTM C518): Not less than 0.56.




i.
Nail Pull Resistance (ASTM C1396): Not less than 90.




j.
Hardness, Core, Edges, and Ends (ASTM C1396): Greater than 15.




k.
Acceptable Products:





1)
ToughRock Fireguard C.





2)





3)







PARAGRAPH BELOW IS 5/8 INCH TOUGHROCK FIREGUARD.



3.
Fire-Rated Paper Faced Gypsum Board:




a.
Thickness: 5/8 inch.




b.
Width: 4 feet.




c.
Length: 8 feet.




d.
Weight: 2200 pounds per M square feet.




e.
Edges: [Tapered] [Square] [Rounded].




f.
Flexural Strength, Parallel (ASTM C1396): 50 pounds per square inch.




g.
Flexural Strength, Perpendicular (ASTM C1396): 150 pounds per square inch.




h.
R-Value (ASTM C518): 0.56.




i.
Nail Pull Resistance (ASTM C1396): Not less than 90 lbf.




j.
Hardness, Core, Edges, and Ends (ASTM C1396): Greater than 15 lbf.




k.
Acceptable Products:





1)
5/8" ToughRock Fireguard.







PARAGRAPH BELOW IS 1/2 INCH DENSARMOR PLUS FIREGUARD C.



4.
Fire-Rated Fiberglass-Mat Faced Gypsum Board:




a.
Thickness: 1/2 inch.




b.
Width: 4 feet.




c.
Length: 8 feet.




d.
Weight: 2100 pounds per M square feet.




e.
Edges: Tapered.




f.
Surfacing: Coated fiberglass mat on face, back, and long edges.




g.
Flexural Strength, Parallel (ASTM C1396, C1658): 80 lbf.




h.
Flexural Strength, Perpendicular (ASTM C1396, C1658): 100 lbf.




i.
R-Value (ASTM C518): 0.56.




j.
Nail Pull Resistance (ASTM C1396, C1658): Not less than 80 lbf.




k.
Hardness, Core, Edges, and Ends (ASTM C1396): Greater than 15 lbf.




l.
Water Absorption (ASTM C1396): 5 percent of weight maximum.




m.
Mold Resistance (ASTM D3273): 10, in a test as manufactured.



n.
Acceptable Products:





1)
1/2" DensArmor Plus Fireguard C, Georgia-Pacific Gypsum.





2)





3)







PARAGRAPH BELOW IS 5/8 INCH DENSARMOR PLUS FIREGUARD.



5.
Fire-Rated Fiberglass-Mat Faced Gypsum Board:




a.
Thickness: 5/8 inch.




b.
Width: 4 feet.




c.
Length: 8 feet.




d.
Weight: 2500 pounds per M square feet.




e.
Edges: Tapered.




f.
Surfacing: Coated fiberglass mat on face, back, and long edges.




g.
Flexural Strength, Parallel (ASTM C1396, C1658): 100 pounds per square inch.




h.
Flexural Strength, Perpendicular (ASTM C1396, C1658): 140 pounds per square inch.




i.
R-Value (ASTM C518): 0.67.




j.
Nail Pull Resistance (ASTM C1658): Not less than 90 lbf.




k.
Hardness, Core, Edges, and Ends (ASTM C1396): Greater than 15 lbf.




l.
Water Absorption (ASTM C1396): 5 percent of weight maximum.




m.
Mold Resistance (ASTM D3273): 10, in a test as manufactured.




n.
Acceptable Products:





1)
5/8" DensArmor Plus Fireguard, Georgia-Pacific Gypsum.





2)





3)

2.03
ACCESSORIES


A.
Fasteners:



1.
Screws: ASTM C1002, corrosion resistant when specified.



2.
Track Fasteners: Power-driven fasteners of size and material capable of withstanding loads imposed on shaftwall assemblies without exceeding allowable design stress of track, fasteners, of structural substrates in which anchors are embedded.




a.
Expansion Anchors (ASTM E488): Fabricated from corrosion-resistant materials and capable of withstanding a load equal to 5 times design load.




b.
Power-Actuated Anchors (ASTM E1190): Fabricated from corrosion-resistant materials and capable of withstanding a load equal to 10 times design load.


B.
Trim: ASTM C1047.







SELECT TRIM MATERIAL AND SHAPES REQUIRED BELOW.



1.
Material: [Galvanized or aluminum-coated steel sheet, rolled zinc, plastic, or paper-faced galvanized steel sheet] [Galvanized or aluminum-coated steel sheet or rolled zinc] [Plastic] [Paper-faced galvanized steel sheet].



2.
Shapes:




a.
Cornerbead.




b.
Bullnose bead.




c.
L-C bead, J-shaped with exposed long flange to receive joint compound.




d.
L bead, L-shaped with exposed long flange to receive joint compound.




e.
U-bead, J-shaped with exposed short flange to receive joint compound.




f.
Control joint.




g.
Curved-edge cornerbead with notched or flexible flanges.


C.
Joint Tape: ASTM C475, 2-1/6-inch-wide paper tape.


D.
Joint Compound: ASTM C475, all-purpose, ready-mixed, vinyl-based.

PART
3
EXECUTION

3.01
EXAMINATION


A.
Verification of Conditions: Verify that site conditions and substrates are acceptable to begin the work of this Section.

3.02
INSTALLATION


A.
General: In accordance with ASTM C840, GA-216, and the manufacturer’s recommendations.

IF OTHER MANUFACTURERS WERE ADDED IN PART 2, REFERENCE THEIR INSTALLATION RECOMMENDATIONS BELOW BY TITLE.



1.
Manufacturer’s Recommendations:




a.
Current “Product Catalog”, Georgia-Pacific Gypsum.




b.



c.







SELECT LEVEL REQUIRED BELOW. IF MORE THAN ONE LEVEL IS REQUIRED, ADD AN INDICATION OF LOCATIONS TO THE PARAGRAPHS RETAINED BELOW OR ADD A SCHEDULES ARTICLE TO INDICATE LOCATIONS.

B.
Finishing: In accordance with GA-214, Level as indicated below:



1.
[Level 0] [Level 1] [Level 2] [Level 3] [Level 4] [Level 5].

3.03
PROTECTION

REVISE BELOW IF OTHER THAN AIA GENERAL CONDITIONS ARE USED.


A.
Protect gypsum board installations from damage and deterioration until the date of Substantial Completion.







RETAIN ARTICLE BELOW IF A SCHEDULE IS REQUIRED FOR FINISH LEVELS.

3.04
SCHEDULES

END OF SECTION 09 21 16.23


Gypsum Board

Project Name/Number/Date
09 21 16.23-

Shaft Wall Assemblies


