# FUNCTIONAL CHARACTERISTICS

| This series is made of highly resistant, extremely durable IF 727 material. Featuring an ergonomic design, it has an opening at the back and the backrest flexes according to the user's need for support. This is achieved without any kind of mechanism or springs thanks to the quality of the materials employed. The basic K-7129 version, also made of IF 727, has a non-slip pattern on the front of the seat. All the versions are stackable and a trolley is optionally available to make moving them easy and convenient once they have been stacked. This series is also available in a T2 version with seat and backrest upholstered in fire-resistant fabrics. The upholstery is mounted on a wooden backing that is riveted to the seat and is easily replaceable. This series incorporates a linking system that enables the formation of straight or gently curved rows. Optionally rows can be made up of alternate K-1729 and K-7130 models in order to obtain a single common armrest between seats. |  |
| --- | --- |

The metal structures of this series are made of oval steel tubing painted with black powder epoxy paint, although they are optionally available in grey.

All these features make this an exceptionally versatile series for use in different types of areas.

TECHNICAL CHARACTERISTICS

Structures:

Shielded seam arc-welded steel tubing and plate.

Polypropylene:

Material: Polypropylene copolymer IF-727

Mechanical characteristics:

-	Fracture strength DIN 53455  125 MM/Min:250Kp/cm2

-	Impact strength: test piece notched at 23ºC  ISO 179: 13MJ m2

Tests on shells:

- Rigidity, twisting and flexion tests, DIN 68872

Paint:

Electrostatic powder epoxy

Coating thickness: 70-80 microns.

Grid adherence: ISO 2409: 100%

Upholstery:

Fire tests:

-	Standards: UNE/23727: M-1 CSE/RF  4/83:M1

-	NF/P 92507: M1  DIN 4102 part 1: B1

-	BS 5182 parts 1 and 2 (with fire barrier)

-	Pilling index: 5 BS 5811