GYPSUM CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR DURA-CAP FLOOR UNDERLAYMENT AS AN ENCLOSURE OVER AN ASBESTOS SOIL-PENETRATING ENCAPSULANT IN SOIL FLOORED CRAWL SPACE OR TUNNEL AREAS

PART 1	GENERAL

1.01		SUMMARY

- This is the recommended specification for Dura-Cap Floor Underlayment as an enclosure over an asbestos soil-penetrating encapsulant in soil floored crawl space or tunnel areas.

1.02			SECTION INCLUDES

- Dura-Cap gypsum cement

- Maxxon Set Modifier

1.03			QUALITY ASSURANCE

- Installer's Qualifications:  Installation of Dura-Cap shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04		DELIVERY, STORAGE AND HANDLING

- General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05		SITE CONDITIONS

- Environmental Requirements:  Before, during and after installation of Dura-Cap, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2	PRODUCTS

2.01		MATERIALS

- Cementitious Flooring:  Dura-Cap gypsum cement as manufactured by Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

- Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specification 101.

- Mix Water:  Potable, free from impurities.

2.02		MIX DESIGNS

- General Requirements:  Dura-Cap mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3	EXECUTION

3.01	CRAWL SPACE OR TUNNEL PREPARATION

- Abatement contractor:  Shall be responsible for soil encapsulation prior to the Dura-Cap application.  Abatement contractor shall apply EPA approved bridging encapsulant.

- Cure Time:  The cure time of bridging encapsulant depends on environmental conditions.  Typically it takes 8-12 hours to cure, after this time, the Dura-Cap application may begin.

3.02	APPLICATION OF CEMENTITIOUS FLOORING

- Dura-Cap Application:  The soil floor in the crawl space or tunnel must be free of all friable asbestos and the penetrating encapsulant must be fully cured.  A nominal 2 inch (50 mm) layer of Dura-Cap is then installed.  The Dura-Cap will be installed in two 1 inch (25 mm) applications [two lifts].  This will allow the first 1 inch (25 mm) of Dura-Cap to fill in low areas and enclose any floating materials.  The second 1 inch (25 mm) layer of Dura-Cap will make a smooth finish and completely enclose the soil floor.  Note:  Maxxon Set Modifier may be used to accelerate the set time of the first lift.

- Drying:  General Contractor shall provide continuous ventilation and adequate heat to rapidly remove moisture from the area until the Dura-Cap is dry.  General Contractor shall provide mechanical ventilation if necessary.

3.03	FIELD QUALITY CONTROL

- Slump Test:  Dura-Cap mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 8 inches (203 mm) plus or minus 1 inch (25 mm) diameter.

- Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Dura-Cap application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 472.  Test results shall be available to architect and/or contractor upon request from applicator.

END OF SECTION