GYPSUM CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR COMMERCIAL TOPPING( “GREEN” FLOOR UNDERLAYMENT OVER PRECAST CONCRETE SLABS

PART 1
GENERAL

1.01

SUMMARY


A.
This is the recommended specification for Commercial Topping “Green” Floor Underlayment over precast concrete slabs.

1.02


SECTION INCLUDES

A. Commercial Topping “Green” floor underlayment with fly ash a non-combustible mineral portion of coal generated in a coal combustion power plant

     
USGBC LEED Credit Areas Impacted by Commercial Topping “Green” Floor Underlayment

	Project
	Category
	Credit

	Indoor Environmental Quality
	Low Emitting Materials
	EQ 4.1       <0.24 mg/m3
                 GREENGUARD Compliant
                 for Indoor Air Quality Certified®  

	Materials & Resources
	Recycled Content
 

Local/Regional Materials
 

Local/Reg. Materials
	MR 4.1 – 4.2     Fly Ash 
 

MR 5.1      Blue Rapids, KS   66411
                  Camden, NJ 08103
                  Brunswick, GA 31521             
                  Las Vegas, NV 89124 

 MR 5.2      Job site manufactured 
                   with local sand & water    


B. Maxxon Floor Primer

C. Maxxon Overspray

1.03


QUALITY ASSURANCE

A. Installer's Qualifications:  Installation of Commercial Topping “Green” shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Commercial Topping “Green”, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and precast temperature are stabilized.

PART 2
PRODUCTS

2.01

MATERIALS

A. Commercial Topping “Green” gypsum cement:  Floor underlayment compound shall be Commercial Topping “Green” gypsum cement underlayment as manufactured by Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

B. Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specification 101.

C. Mix Water:  Potable, free from impurities.

D. Precast Primer:  Maxxon Floor Primer

E. Sealer:  Maxxon Overspray

2.02

MIX DESIGNS

A. General Requirements:  Commercial Topping “Green” mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Precast:  Precast shall be structurally sound.  General Contractor shall clean precast to remove mud, oil, grease, and other contaminating factors before arrival of the Commercial Topping “Green” underlayment crew.

B. Leak Prevention:  Fill cracks and voids with a quick setting caulk or patching material where leakage of Commercial Topping “Green” could occur.

C. Priming Precast:  Prime precast using the Maxxon Floor Primer.  Priming instructions vary according to the porosity of the precast, multiple coats may be necessary.

D. Expansion Joints:  Allow joints to continue through the Commercial Topping “Green” at the same width.

3.02
APPLICATION OF CEMENTITIOUS FLOORING

A. Scheduling:  Application of Commercial Topping “Green” shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

B. Application:  Place Commercial Topping “Green” from 3” (76 mm) to featheredge.  Spread and float Commercial Topping Green to a smooth surface.  Except at authorized joints, place Commercial Topping “Green” as continuously as possible until application is complete so that no Commercial Topping “Green” slurry is placed against Commercial Topping “Green” product that has obtained its initial set.

C.  Drying:  General Contractor shall provide continuous ventilation and adequate heat to rapidly      remove moisture from the area until the Commercial Topping “Green” is dry.  General Contractor shall provide mechanical ventilation if necessary.  Under the above conditions, for 3/4 inch (19 mm) thick Commercial Topping “Green”, 5-7 days is usually adequate drying time.  To test for dryness, tape a 24 inch by 24 inch (609 mm by 609 mm) section of plastic or high density rubber mat to the surface of the underlayment.  After 48-72 hours, if no condensation occurs, the underlayment shall be considered dry.  Perform dryness test 5‑7 days after pour.

3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Sealing:  Seal all areas that receive glue down floor goods with Maxxon Overspray according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used. Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

B. Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL

A. Slump Test:  Commercial Topping “Green” mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 8 inches (203 mm) plus or minus 1 inch (25 mm) diameter.

B. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Commercial Topping “Green” application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 472.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Commercial Topping “Green” wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION

72

