GYPSUM CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR COMMERCIAL TOPPING( FLOOR UNDERLAYMENT OVER WOODEN SUBFLOORS

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Commercial Topping Floor Underlayment over wooden subfloors.

1.02


SECTION INCLUDES

A. Commercial Topping Floor Underlayment

B. Maxxon Floor Primer

C. Maxxon Moistop

D. Maxxon Surface Conditioner

E. Maxxon Overspray

F. Mesh Reinforcement

1.03


QUALITY ASSURANCE

A. Installer's Qualifications:  Installation of Commercial Topping shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Commercial Topping, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperature are stabilized.  

PART 2
PRODUCTS

2.01 MATERIALS

A. Cementitious Self-Leveling Poured Floor Underlayment:  Floor underlayment compound shall     be Commercial Topping Self-Leveling Floor Underlayment as manufactured by Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

B. Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specification 101.

C. Mix Water:  Potable, free from impurities.

D. Subfloor Primer:  Maxxon Floor Primer.

E. Sealer:  Maxxon Overspray

F. Wood Subfloor Sealer:  Maxxon Surface Conditioner, Maxxon Overspray, or use a slipsheet such as Maxxon Moistop.

G. Mesh Reinforcement:  Galvanized diamond metal lath mesh.

2.02

MIX DESIGNS

A. General Requirements:  Commercial Topping mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Wooden Subfloor:  The wooden subfloor must be fully secured, nailed or screwed, structurally sound and broom clean.  Deflection shall not exceed L/360th of the span including live and dead loads.  Fill cracks and holes in the floor with crack filler or caulk.

B. Seal the Wooden Subfloor:  The day before the pour, seal the wood with 1-2 coats of 
Maxxon Surface Conditioner or Maxxon Overspray diluted 1:1 with water sprayed, rolled or broomed on at 300 sq. ft./gal (7.3 m2/L), or staple a slipsheet such as Maxxon Moistop across the entire wood floor.

C. Prime the Wooden Subfloor:  The wood subfloor must be primed.  Prime the sealed subfloor with Maxxon Floor Primer following Maxxon bonding procedures #109.  If a slipsheet is used, the subfloor does not have to be primed.

D. Mesh Reinforcement:  Staple a thin (2.5 or 3.4 lb./sq. yd.), galvanized diamond metal lath mesh to the subfloor, overlapping the lath where it meets.  This is done across the entire floor.

E. Expansion Joints:  Allow joints to continue through the Commercial Topping at the same width.

3.02
APPLICATION OF CEMENTITIOUS FLOORING

A. Scheduling:  Application of Commercial Topping shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

B. Application:  Place Commercial Topping at 3/4" (19 mm) minimum over the surface of the wooden subfloor.  Spread and screed Commercial Topping to a smooth surface.  Except at authorized joints, place Commercial Topping as continuously as possible until application is complete so that no Commercial Topping slurry is placed against Commercial Topping product that has obtained its initial set.

C. Drying:  General Contractor shall provide continuous ventilation and adequate heat.  With 
Commercial Topping there's no extensive curing time.  Other floor goods can be installed once Commercial Topping passes a moisture test.

3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Sealing:  Seal all areas that receive glue down floor goods with Maxxon Overspray according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

B. Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL

A. Slump Test:  Commercial Topping mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 8 inches (203 mm) plus or minus 1 inch (25 mm) diameter.

B. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Commercial Topping application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Commercial Topping wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION


