GYPSUM CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR COMMERCIAL TOPPING( FLOOR UNDERLAYMENT FOR TOPPING GALVANIZED CORRUGATED STEEL DECK OVER DIETRICH INDUSTRIES, INC. LIGHT-GAUGE STEEL FRAMING 

UL 2-HOUR FIRE DESIGN

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Commercial Topping Floor Underlayment for topping galvanized corrugated steel deck over light-gauge steel framing.

1.02


SECTION INCLUDES

B. Commercial Topping Gypsum Concrete

B. Maxxon Acrylic

C. Galvanized Corrugated Steel Deck

D. Light-Gauge Steel Framing

E. Optional Maxxon Sound Mats:  Acousti-Mat II or Enkasonic.  Or Acousti-Mat 3 reinforced with Maxxon Crack Suppression Mat (CSM).

F. Maxxon Overspray

1.03


QUALITY ASSURANCE

A. Commercial Topping Installer's Qualifications:  Installation of Commercial Topping shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Commercial Topping, building interior shall be enclosed including installation of roof, windows or other apertures and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2
PRODUCTS

2.01

MATERIALS

A. Floor Underlayment:  Commercial Topping gypsum cement as manufactured by Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

B. Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting the requirements of Maxxon Corporation Sand Specification 101.

C. Mix Water:  Potable, free from impurities.

D. Galvanized Corrugated Steel Deck Primer:  Maxxon Acrylic as manufactured by Maxxon Corporation, Hamel, MN. 

E. Galvanized Corrugated Steel Deck:  Galvanized corrugated steel deck conforming to Steel Deck Institute requirements and meeting L/360 design deflection limitation: minimum 22-gauge (9/16’’ Form Deck) required.

F. Light-Gauge steel Framing: Dietrich TradeReady C-shaped, No 16 MSG galvanized steel sections, 9 ¼’’ minimum depths with 1-7/8’’ minimum flanges and ½’’ minimum stiffening flanges as manufactured by Dietrich Industries Inc.

G. Optional Sound Mats:  The following sound mats are listed and optional in the G 560 fire design: Acousti-Mat II or Enkasonic.  Or Acousti-Mat 3 reinforced with Maxxon Crack Suppression Mat (CSM).  All manufactured by Maxxon Corporation, Hamel, MN.

H. Floor Underlayment Sealer:  Maxxon Overspray as manufactured by Maxxon Corporation, Hamel, MN.

2.02

MIX DESIGNS

A. General Requirements:  Commercial Topping mix proportions and methods shall be in strict accordance with product manufacturer recommendations. 

PART 3
EXECUTION

3.01
PREPARATION

A. Structure:  Structure shall meet Maxxon Corporation’s minimum deflection requirements as well as other structural standards, and be certified by a licensed structural engineer.

B. Condition and Cleaning Galvanized Corrugated Steel Deck:  Galvanized corrugated steel deck shall be structurally sound.  General Contractor shall clean to remove mud, oil, grease and other contaminating factors before arrival of the Commercial Topping underlayment crew.

C. Leak Prevention:  All potential leakage areas including pipe penetrations, screw holes and laps must be caulked.

D. Priming Corrugated Steel Deck:  Prime corrugated steel deck using the Maxxon Acrylic. 

E. Expansion Joints:  Allow joints to continue through the Commercial Topping at the same width.

3.02
APPLICATION OF CEMENTITIOUS FLOORING

A. Scheduling:  Application of Commercial Topping shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

B. Application:  Place Commercial Topping at 1 inch (25 mm) minimum over the top of the flutings, average pour thickness is 1-9/16’’ (40 mm).  Spread and screed Commercial Topping to a smooth surface.  Except at authorized joints, place Commercial Topping as continuously as possible until application is complete so that no Commercial Topping slurry is placed against Commercial Topping product that has obtained its initial set.

C. Application of Optional Sound Mats:  If this option is chosen it replaces B above.  Place Commercial Topping over the tops of the flutings to a smooth surface.  Once the Commercial Topping reaches full set (2-4 hours) install     Acousti-Mat II, Enkasonic or Acousti-Mat 3 per manufacturer’s recommendations.  Commercial Topping thickness over Acousti-Mat II is 1” (25mm), over Enkasonic 1 ½” (38mm).  Commercial Topping thickness over Acousti-Mat 3 is 1 ½” (38 mm), reinforced with Maxxon CSM.    

D. Drying:  General Contractor shall provide continuous ventilation and adequate heat to rapidly remove moisture from the area until the Commercial Topping is dry.  General Contractor shall provide mechanical ventilation if necessary.  Under the above conditions, for 1-9/16’’ (40 mm) thick Commercial Topping, 10-14 days is usually adequate drying time.  To test for dryness, tape a 24 inch by 24 inch (609 mm by 609 mm) section of plastic or high density rubber mat to the surface of the underlayment.  After 48-72 hours, if no condensation occurs, the underlayment shall be considered dry.  Moisture meters such as Delmhorst    G-79 or BD 21000 can be used; also Relative Humidity Probes are acceptable.  Perform dryness test 10-14 days after pour.

3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS


A.
Priming:  Prime all areas that receive glue down floor goods according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and primed regardless of floor covering to be used.  Use Maxxon Floor Primer or Maxxon Overspray to prime the Commercial Topping prior to installation of glue down floor goods.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.


B.
Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL


A.
Slump Test:  Commercial Topping mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 8-1/2 inches (216 mm) plus or minus 1 inch 


(25 mm) diameter.


B.
Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Commercial Topping application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with ASTM C 472.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05
PROTECTION


A.
Protection From Heavy Loads:  During construction, place temporary wood planking over 
Commercial Topping wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION
