SELF-LEVELING CONCRETE FLOOR UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT FLOOR UNDERLAYMENT OVER MAXXON® MOISTOP FOR OLD WOOD FRAME CONSTRUCTION

PART 1	GENERAL

1.01		SUMMARY

- This is the recommended specification for Level-Right Floor Underlayment over Maxxon Moistop for old wood frame construction.

1.02			SECTION INCLUDES

- Level-Right Cementitious Underlayment

- Maxxon Floor Primer

- Maxxon Overspray

- Maxxon Moistop

- Reinforcement Mesh

1.03			QUALITY ASSURANCE

- Installer's Qualifications:  Installation of Level-Right shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04		DELIVERY, STORAGE AND HANDLING

- General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05		SITE CONDITIONS

- Environmental Requirements:  Before, during and after installation of Level-Right and Maxxon Moistop, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2	PRODUCTS

2.01		MATERIALS

- Cementitious Cement:  Floor underlayment Level-Right cementitious underlayment as manufactured by Maxxon Corporation, Hamel, MN.

- Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specification 101.

- Maxxon Moistop:  Fiberglass reinforced membrane coated on both sides with polyethylene.

- Mix Water:  Potable, free from impurities.

- Subfloor Primer:  Maxxon Floor Primer, a special Ethylene Vinyl Acetate Copolymer Emulsion.

- Sealer:  Maxxon Overspray

- Reinforcement mesh:  Galvanized metal lath (3.4 lbs./sq.yd.) or Maxxon Plastic Reinforcement Net.

2.02		MIX DESIGNS

- General Requirements:  Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3	EXECUTION

3.01	PREPARATION

- Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before arrival of the Level-Right underlayment crew.

- Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of Level-Right could occur.

- Maxxon Moistop Installation:  Roll out Moistop across the entire old wood subfloor overlapping joints approximately 6 inches (152 mm).  Secure Moistop using a frequency of staples to adequately pull the Moistop tight to the wood subfloor.  Overlap must be stapled every 4 – 6 inches (101 mm to 152mm) to maintain a tight seam.  Floor penetration should be filled or caulked.

- Priming Subfloor:  Prime the subfloor using the Maxxon Floor Primer.

## Reinforcement Mesh: Galvanized metal lath (3.4 lbs./sq.yd.) must be laid across the entire      floor, overlapped and stapled through Moistop to the wood subfloor.

3.02	APPLICATION OF SELF-LEVELING FLOORING

- Scheduling:  Application of Level-Right shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation.

- Application:  Place Level-Right ¾ inch (19mm) minimum over Moistop and reinforcement lath.

- Drying:  General Contractor shall provide continuous ventilation and adequate heat.  General Contractor shall provide mechanical ventilation if necessary.   To test for dryness, tape a 24 inch by 24 inch (609 mm by 609 mm) section of plastic or high density rubber mat to the surface of the underlayment.  After 48-72 hours, if no condensation occurs, the underlayment shall be considered dry.  Perform dryness test 5-7 days after pour.

3.03	PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

- Sealing:  Seal all areas that receive glue down floor goods with Maxxon Overspray according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used. Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

- Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04	FIELD QUALITY CONTROL

- Slump Test:  Level-Right mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 9 inches (229 mm) plus or minus 1 inch (25 mm) diameter.

- Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right application.  Cubes shall be tested by the Maxxon Corporation in accordance with ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05	PROTECTION

- Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION