SELF-LEVELING CONCRETE FLOOR UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( PLUS CEMENTITIOUS SELF-LEVELING FLOOR UNDERLAYMENT FOR CAPPING LIGHTWEIGHT CONCRETE

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Level-Right Plus Cementitious Self-Leveling Floor Underlayment for capping lightweight concrete.

1.02


SECTION INCLUDES

A. Level-Right Plus Cementitious Self-Leveling Floor Underlayment

B. Maxxon Floor Primer

C. Maxxon Acrylic

D. Maxxon Overspray

1.03


QUALITY ASSURANCE

A. Installer's Qualifications:  Installation of Level-Right Plus shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Level-Right Plus, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperature are stabilized.

PART 2
PRODUCTS

2.01

MATERIALS

A. Cementitious Self-Leveling Poured Floor Underlayment:  Floor underlayment compound shall be Level-Right Plus Self-Leveling Floor Underlayment as manufactured by Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

B. Sand Aggregate:  Sand shall be silica aggregate meeting requirements of Level-Right Plus Sand Specification 101.

C. Mix Water:  Potable, free from impurities.

D. Subfloor Primer:  Maxxon Floor Primer

E. Sealer:  Maxxon Overspray

F. Lightweight Concrete sealer:  Maxxon Overspray or Maxxon Acrylic

2.02

MIX DESIGNS


A.
General Requirements:  Level-Right Plus mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Lightweight Concrete: Allow the lightweight concrete to cure for 28 days before the Level-Right Plus application. The surface and cracks in the lightweight concrete must be vacuumed free of all dirt, dust and debris.  

B. Seal the Lightweight Concrete:  Seal the lightweight concrete using Maxxon Overspray or Maxxon Acrylic.  Follow Maxxon Corporation's recommendations for dilution ratio and coverage rates.  Multiple coats may be necessary depending on the lightweight concrete porosity.

C. Prime the Lightweight Concrete:  Prime the lightweight concrete using the Maxxon Floor Primer.  Follow Maxxon Corporation's recommendations for dilution and coverage rates.

D. Expansion Joints:  Allow joints to continue through the Level-Right Plus at the same width.

3.02
APPLICATION OF SELF-LEVELING FLOORING

A. Scheduling:  Application of Level-Right Plus shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

B. Application:  Place Level-Right Plus at 3/8 inch (10 mm) minimum over the surface of the lightweight concrete.  Spread and screed Level-Right Plus to a smooth surface.  Except at authorized joints, place Level-Right Plus as continuously as possible until application is complete so that no Level-Right Plus product slurry is placed against Level-Right Plus product that has obtained its initial set. 

C. Drying:  General Contractor shall provide continuous ventilation and adequate heat.  With 
Level-Right Plus there's no extensive curing time.  Ceramic tile can be thin set within 2 to 4 hours.  Other floor goods can be installed once the underlayment is dry.

3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL

A. Slump Test:  Level-Right Plus mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 9 1/2 inches (241 mm) plus or minus 1 inch (25 mm) diameter.

B. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right Plus application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right Plus wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION


