SELF-LEVELING CONCRETE FLOOR UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( PLUS CEMENTITIOUS FLOOR UNDERLAYMENT FOR TOPPING WOOD SUBFLOORS USING REINFORCEMENT

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Level-Right Plus Cementitious Floor Underlayment for topping wood subfloors using reinforcement.

1.02


SECTION INCLUDES

A. Level-Right Plus cementitious floor underlayment

B. Reinforcement mesh

C. Maxxon Moistop or wood sealers

D.  Maxxon Floor Primer
E.  Maxxon Overspray
F.  Maxxon Acrylic Sealer

1.03


QUALITY ASSURANCE

A. Installer's Qualifications:  Installation of Level-Right Plus shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Level-Right Plus, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2
PRODUCTS

2.01

MATERIALS

A. Cementitious Floor Underlayment:  Floor underlayment compound shall be Level-Right Plus cementitious underlayment as manufactured by Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

B. Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry, plaster, or silica sand meeting requirements of Level-Right Plus Sand Specification 101.

C. Mix Water:  Potable, free from impurities.

D. Slip Sheet or Wood Sealers:  Maxxon Moistop, Maxxon Overspray or Maxxon Acrylic Sealer.

E. Reinforcement:  Galvanized diamond metal lath mesh

F.  Subfloor Primer:  Maxxon Floor Primer (Ethylene - vinyl acetate copolymer)

2.02

MIX DESIGNS

A. General Requirements:  Level-Right Plus mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Wood Subfloor:  Subfloor shall be structurally sound. General contractor shall fasten down any loose boards and remove and replace any weak areas.  They shall also clean subfloor to remove mud, oil, grease, and other contaminating factors before arrival of the Level-Right Plus underlayment crew.

B. Leak prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of Level-Right Plus could occur.

C. Install Slip Sheet or Wood Sealers:  Lay out Maxxon Moistop across the entire wood subfloor overlapping and stapling until Maxxon Moistop is completely flat, or install application of Maxxon Acrylic or Maxxon Overspray to seal the subfloor.

D. Install Reinforcement:  Lay out the galvanized metal lath across the entire floor slightly overlapping all seams.  Staple securely through the slip sheet into the wood subfloor.

E. Priming Slip Sheet or Wood Sealers:  Prime the slip sheet or wood sealers using the Maxxon Floor Primer per manufacturer’s recommendations.

F. Expansion Joints:  Allow joints to continue through the Level-Right Plus at the same width.

3.02
APPLICATION OF CEMENTITIOUS FLOORING

A. Scheduling:  Application of Level-Right Plus shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

B. Application:  Place Level-Right Plus at 3/4" (19 mm) over the surface of the slip sheet and metal lath.  Spread and screed Level-Right Plus to a smooth surface.  Except at authorized joints, place Level-Right Plus as continuously as possible until application is complete so that no 
Level-Right Plus slurry is placed against Level-Right Plus product that has obtained its initial set.

C. Drying:  General Contractor shall provide continuous ventilation and adequate heat to rapidly remove moisture from the area until the Level-Right Plus is dry.  General Contractor shall provide mechanical ventilation if necessary.

3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL

A. Slump Test:  Level-Right Plus mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 9 inch (229 mm) plus or minus 1 inch (25 mm) diameter.

B. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right Plus application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right Plus wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION


