SELF-LEVELING CONCRETE FLOOR UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( FS-10 CEMENTITIOUS 
SELF-LEVELING FLOOR UNDERLAYMENT FOR TOPPING CONCRETE FLOORS

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Level-Right FS-10 Cementitious Self-Leveling Floor Underlayment for topping concrete floors.

1.02


SECTION INCLUDES

A. Level-Right FS-10 Cementitious Self-Leveling Floor Underlayment

B. Manufacturer Approved Primer

1.03


QUALITY ASSURANCE

A. Installer's Qualifications:  Installation of Level-Right FS-10 shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Level-Right FS-10, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperature are stabilized.

PART 2
PRODUCTS

2.01

MATERIALS

A. Cementitious Self-Leveling Poured Floor Underlayment:  Floor underlayment compound shall be Level-Right FS-10 Cementitious Self-Leveling Floor Underlayment as manufactured by Maxxon Corporation, Hamel, MN.

B. Mix Water:  Potable, free from impurities.

C. Concrete Primer:  Manufacturer Approved Primer

D. Sealer:  Manufacturer Approved Sealer

2.02

MIX DESIGNS

A. General Requirements:  Level-Right FS-10 mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  Steel troweled concrete, concrete sealed with curing compounds, or slick or smooth substrate surfaces must be shotblast or scarified.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before arrival of the Level-Right FS-10 underlayment crew.

B. Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of Level-Right FS-10 could occur.

C. Priming Subfloor:  Prime concrete subfloor using the Manufacturer Approved Primer.  Priming instructions vary according to the porosity of the concrete, multiple coats may be necessary.

D. Expansion Joints:  Allow joints to continue through the Level-Right FS-10 at the same width.

3.02
APPLICATION OF SELF-LEVELING FLOORING

A. Scheduling:  Application of Level-Right FS-10 shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

B. Application:  Place Level-Right FS-10 0 - 3/8” (0 - 10 mm).  Spread and float Level-Right
FS-10 to a smooth surface.  Except at authorized joints, place Level-Right FS-10 as continuously as possible until application is complete so that no Level-Right FS-10 slurry is placed against Level-Right FS-10 product that has obtained its initial set.

C. Drying:  General Contractor shall provide continuous ventilation and adequate heat until 
Level-Right FS-10 is dry.  General contractor shall provide mechanical ventilation if necessary.

3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Floor Goods Attachment:  See the brochure "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL

A. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right FS-10 application.  Cubes shall be tested as recommended by the
Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right FS-10 wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION

