SELF-LEVELING CEMENTITIOUS TOPPING
RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( WEARTOP CEMENTITIOUS 
SELF-LEVELING FLOOR TOPPING FOR CAPPING CONCRETE FLOORS 

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Level-Right WearTop Cementitious Self-Leveling Floor Topping for capping concrete floors.

1.02


SECTION INCLUDES

A. Level-Right WearTop Cementitious Self-Leveling Floor Topping

B. Manufacturer Approved Primer

C. Maxxon WearTop Curing Agent
D. Manufacturer Approved Sealer or Wax
1.03


QUALITY ASSURANCE

A. Installer's Qualifications:  Installation of Level-Right WearTop shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Level-Right WearTop, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperature are stabilized.

PART 2
PRODUCTS

2.01

MATERIALS

B. Cementitious Self-Leveling Poured Floor Topping:  Floor topping compound shall be 
Level-Right WearTop Cementitious Self-Leveling Floor Topping as manufactured by 
Maxxon Corporation, Hamel, MN.

B. Mix Water:  Potable, free from impurities.

C. Concrete Primer:  Manufacturer Approved Primer

D. Curing Agent:  Maxxon WearTop Curing Agent
E. Sealer:  Manufacturer Approved Sealer or Wax
2.02

MIX DESIGNS

A. General Requirements:  Level-Right WearTop mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Concrete:  Concrete shall be structurally sound. Steel troweled concrete, concrete sealed with curing compounds, or slick or smooth substrate surfaces must be shotblast or scarified to a Concrete Surface Profile of 5 (CSP 5) per International Concrete Repair Institute Guideline 03732.  General Contractor shall clean concrete to remove mud, oil, grease, and other contaminating factors before arrival of the Level-Right WearTop crew.

B. Leak Prevention:  Fill cracks and voids with a quick setting cement patching or caulking material where leakage of Level-Right WearTop could occur.

C. Priming Concrete: Prime concrete using the Manufacturer Approved Primer.  Priming instructions vary according to the porosity of the concrete, multiple coats may be necessary.

D. Expansion Joints:  Allow joints to continue through the Level-Right WearTop at the same width.

3.02
APPLICATION OF SELF-LEVELING FLOORING

A. Scheduling:  Application of Level-Right WearTop shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration. 

B. Application:  Place Level-Right WearTop 0 – 1 inch (0 - 25 mm). Deeper applications can be done in multiple lifts or using stone per manufactures recommendations. Spread and float Level-Right WearTop to a smooth surface.  Except at authorized joints, place Level-Right WearTop as continuously as possible until application is complete so that no Level-Right WearTop slurry is placed against Level-Right WearTop product that has obtained its initial set.

C. Sanding for Burnished, Marble Look:  Buff sand the WearTop surface the day after the pour with a traditional floor buffing machine using an 80, 100 or 120 mesh screen to desired look.  After the surface is screen sanded and broomed, use a tack rag or dry Swiffer mop to remove dust.

D. Curing and Sealing:  Level-Right WearTop is to be coated with at least 2 coats of Maxxon WearTop Curing Agent within 24 hours after installation except when an epoxy or other floor coverings will be installed.

E. Sealers and Wax:  Apply sealer or wax after the floor is dust free from sanding.  Follow manufacturer’s instructions.
F. Drying:  General Contractor shall provide continuous ventilation and adequate heat until 
Level-Right WearTop is fully cured.
3.03
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Floor Goods Attachment:  See the brochure "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04
FIELD QUALITY CONTROL

A. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right WearTop application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05 PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right WearTop wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION


