GYPSUM CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR MAXXON® FLOOR UNDERLAYMENT OVER ACOUSTI-MAT( 3 SOUND DEADENING PAD FOR OPEN BEAM CONSTRUCTION

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Maxxon Underlayment over Acousti-Mat 3 sound deadening pad for open beam construction.

1.02


SECTION INCLUDES

A. Maxxon Underlayment gypsum cement 

B. Acousti-Mat 3

C. Maxxon Crack Suppression Mat (CSM)

D. Maxxon Floor Primer

E. Maxxon Overspray

F. Maxxon Moistop

1.03


QUALITY ASSURANCE

A. Maxxon Floor Underlayment Installer's Qualifications:  Installation of Maxxon Floor Underlayment shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

B. Acousti-Mat 3 Installer's Qualifications:  Installation of Acousti-Mat 3 shall be by an applicator authorized by the Maxxon Corporation.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Maxxon Floor Underlayment and Acousti-Mat 3, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2
PRODUCTS

2.01

MATERIALS

A. Gypsum Cement:   Maxxon Floor Underlayment gypsum cement as manufactured by the Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

B. Sound Deadening Pad:  Acousti-Mat 3 as manufactured by the Maxxon Corporation,
 Hamel, MN.

C. Reinforcement Mesh:  Maxxon Crack Suppression Mat (CSM) or 3.4 lbs./sq. yd. galvanized diamond metal lath.
D. Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specifications 101.

E. Mix Water:  Potable, free from impurities

F. Subfloor Primer:  Maxxon Floor Primer

G. Sealer:  Maxxon Overspray

H. Moisture retarder for old wood subfloors:  Maxxon Moistop as manufactured by Maxxon Corporation, Hamel MN.

2.02

MIX DESIGNS

A. General Requirements:  Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before the arrival of the Maxxon Floor Underlayment crew.

B. Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of Maxxon Floor Underlayment could occur.

C. Expansion Joints:  Allow joints to continue through the Maxxon Floor Underlayment at the same width.

3.02
APPLICATION OF MAXXON MOISTOP AND ACOUSTI-MAT 3

A. Installation of Maxxon Moistop and Acousti-Mat 3:  Install Maxxon Moistop and Acousti-Mat 3 as recommended by the Maxxon Corporation.

3.03
APPLICATION OF CEMENTITIOUS FLOORING

A. Scheduling:  Application of Maxxon Floor Underlayment shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.  If 
Acousti-Mat 3 is to be installed before drywall, then Maxxon Crack Suppression Mat (CSM) or 3.4 lb/sq. yd. galvanized metal lath must be loose laid over the entire Acousti-Mat 3 surface.  Schedule the Acousti-Mat 3 sound control system as late as possible in the construction cycle.









B. Priming Acousti-Mat 3:  Prime Acousti-Mat 3 using the Maxxon Floor Primer to bond the Maxxon Floor Underlayment to the mat.

C. Maxxon Floor Underlayment Application:  Place Maxxon Floor Underlayment 1 1/2 inches (38 mm) thick over loosely laid Maxxon CSM.  The reinforcement mesh must be overlapped at all seams.  The minimum thickness of Maxxon Floor Underlayment over the Acousti-Mat 3 and Maxxon CSM is l 1/2 inches (38 mm).  Spread and screed the Maxxon Floor Underlayment to a smooth surface.

D. Drying:  General Contractor shall provide continuous ventilation and adequate heat to rapidly remove moisture from the area until the Maxxon Floor Underlayment is dry.  General Contractor shall provide mechanical ventilation if necessary.  Under the above conditions, for 1 1/2 inches thick (38 mm) Maxxon Floor Underlayment, 7-10 days is usually adequate drying time.  To test for dryness, tape a 24 inch by 24 inch (609 mm by 609 mm) section of plastic or a high density rubber mat to the surface of the underlayment.  After 48-72 hours, if no condensation occurs, the underlayment shall be considered dry.  Perform dryness test 5-7 days after pour.

3.04
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Sealing:  Seal all areas that receive glue down floor goods with Maxxon Overspray according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used. Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

B. Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.05
FIELD QUALITY CONTROL

A. Slump Test:  Maxxon Floor Underlayment mix shall be tested for slump as it's being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 8 inches (203 mm) plus or minus 1 inch (25 mm) diameter.

B. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Maxxon Floor Underlayment application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with ASTM C 472.  Test results shall be available to architect and/or contractor upon request from applicator.

3.06
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Maxxon Floor Underlayment wherever it will be subject to heavy wheeled or concentrated loads.









  END OF SECTION

156

