SELF LEVELING CONCRETE FLOOR UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( OVER ACOUSTI-MAT( LP SOUND DEADENING PAD OVER CONCRETE

PART 1
GENERAL

1.01

SUMMARY

A. This is the recommended specification for Level-Right over Acousti-Mat LP sound deadening pad over concrete.

1.02


SECTION INCLUDES

A. Level-Right Cementitious Underlayment
B. Acousti-Mat LP
C. Acousti-Mat LP Adhesive
D. Maxxon Overspray

1.03


QUALITY ASSURANCE

A. Level-Right Installer's Qualifications:  Installation of Level-Right shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

B. Acousti-Mat LP Installer's Qualifications:  Installation of Acousti-Mat LP shall be by an applicator authorized by the Maxxon Corporation.

1.04

DELIVERY, STORAGE AND HANDLING

A. General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05

SITE CONDITIONS

A. Environmental Requirements:  Before, during and after installation of Level-Right and Acousti-Mat LP, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2
PRODUCTS

2.01

MATERIALS

A. Gypsum Cement: Recommended Level-Right Cementitious Underlayment as manufactured by the Maxxon Corporation, Hamel, MN.  
B. Sound Deadening Pad:  Acousti-Mat LP as manufactured by the Maxxon Corporation, Hamel, MN.

C. Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specifications 101.

D. Mix Water:  Potable, free from impurities

E. Adhesive:  Acousti-Mat LP Adhesive as manufactured by the Maxxon Corporation, Hamel, MN.
F. Sealer:  Maxxon Overspray as manufactured by the Maxxon Corporation, Hamel MN.
2.02

MIX DESIGNS

A. General Requirements:  Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3
EXECUTION

3.01
PREPARATION

A. Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before the arrival of the Level-Right and Acousti-Mat LP crew.

B. Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of adhesive could occur.

C. Expansion Joints:  Allow joints to continue through the Level-Right at the same width.

3.02
APPLICATION OF ACOUSTI-MAT LP AND REINFORCEMENT MESH

A. Acousti-Mat LP Installation:  Install Acousti-Mat LP following manufacturer’s recommendations and specifications.

3.03
APPLICATION OF SELF LEVELING FLOORING

A. Scheduling:  Application of Level-Right and Acousti-Mat LP shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour. 
B. Application:  Place the recommended Level-Right a nominal 1/2 inch (12 mm) thick over Acousti-Mat LP.  Spread and screed Level-Right to a smooth surface.
C. Drying:  General Contractor shall provide continuous ventilation and adequate heat.  With Level-Right there’s no extensive curing time.  Ceramic tile can be thin set within 2 to 4 hours.  Other floor goods can be installed once Level-Right passes a moisture test.
3.04
PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Sealing:  Seal all areas that receive glue down floor goods with Maxxon Overspray according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

B. Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.05
FIELD QUALITY CONTROL

A. Slump Test:  Level-Right mix shall be tested for slump as it's being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 9 inches (229 mm) plus or minus 1 inch (25 mm) diameter.

B. Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.06
PROTECTION

A. Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION


