DICHROLAM(

Dichrolam 
PRODUCT IDENTIFICATION AND LIMITATIONS

MANUFACTURER
John Blazy Designs – Dichrolam™ Dichroic Laminates Division 

Parma, OH 

PRODUCT DESCRIPTION
Composition – Dichrolam decorative surfacing / window glazing / lighting diffractor sheet product is a structural (glass) and semi-structural laminated sheet product of glass, acrylic, or polycarbonate composite consisting of substrate, dichroic layering inside and applied to # 2 surface with clear adhesive resin interface.  These custom constructions exhibit transmissive and/or reflective color-changing characteristics.  The “Sea” Series of Dichrolam (Black Sea, Red Burl, Crystal Sea, and Caribbean) have the added property of actual textural wave embossing.  All constructions of Dichrolam create color from the interference principles of thin film physics, therefore they do not have any pigments or dyes, and will not fade in color over time or heat loads up to 290°F.
Category II Safety Glass Certification: 

The laminated glass version of Dichrolam Red and Green (excluding the “Sea” series) passes CPSC 16 CFR 1201 Category II Safety Glass certification, whether annealed or tempered according to American National Standards Z97.1975.  Penetration resistance from the 2.5 KG Ball Drop Test prove equal or higher resistance than standard PVB laminated glass at 48” drop height.  
Heat, humidity, and UV light resistance have all proven to equal and/or exceed that of standard PVB laminated glass.  

The “Sea” Series of Dichrolam (Black Sea, Crystal Sea, and Caribbean) can be specified as safety and / or sloped glazing (skylights) for insulated exterior glass when its construction is a standard Insulated Glass Unit utilizing tempered and laminated glass.  This safety glazing construction uses tempered glass as outboard lite, with standard HS laminated glass with .060” PVB innerlayer as inboard lite with the Dichrolam pattern inside, on # 3 surface.  Total IGU passes sloped glazing codes by the use of code compliant tempered outboard lite and conventional safety laminated inboard lite, and the addition of the Dichrolam layer can only add to the safety/strength/integrity of the total composition.   
The heat, humidity, and UV light resistance of the Dichrolam “Sea” series is made possible through the proprietary Aliphatic Urethane resin formulated by JBD to withstand exterior UV light.  The humidity resistance is controlled through dessicant filled spacers in IG unit construction. 
Fire rating: 
ASTM E-84 smoke density rating – Dichrolam Red and Green  in safety laminated glass has identical fire retarding properties as standard safety laminated glass with PVB innerlayers.   Plastic based Dichrolam can utilize Polycarbonate for better fire ratings instead of Acrylic, when plastics are specified (Class B).
Basic Uses – Available in laminated glass plate form, and various plastics in vertical, horizontal, flooring, flexible and cold forming grades.  It is recommended for interior, as well as some limited exterior applications such as lighting diffractors / louvers, light sculpture, curtainwalls, decorative tiles, signage, point of purchase displays, bar tops, desks, conference tables, occasional furniture, displays or whenever a visually dynamic, full spectrum color shifting appearance is a desirable part of the design concept, whether backlighting or using for opaque surfacing.

LIMITATIONS
Certain JBD dichroic laminates should be specified for interior application only where temperature and humidity levels are normal, unless the construction is designed for exterior use, approved by JBD.  Examples of approved exterior constructions include Dichrolam Red and Green in safety glass laminations where edges can be exposed or sealed in a frame. Dichrolam “Sea Textures” where the construction is an I. G. Unit sealed in a frame.  Use outside of this stipulation is the risk of buyer, based on situational specifics too broad for coverage in this warranty.  Many constructions can be customized for exterior use.     

All other dichroic laminates installed in areas that are subject to constant moisture should be edge sealed with a waterproof sealant such as silicone or butyl type sealants.  Any delamination of non-exterior approved laminates is the risk of buyer.  Aggressive fabricating and cutting techniques increase risk of delamination at buyers risk.  

Due to the unique lamination procedure, optical thin film dichroic core uniqueness, its high reflectivity and said reflectivity’s ability to disguise and hide minor imperfections, the following minor visual aberrations are allowable in the dichroic layer core of these dichroic laminates, not covered under  warranty:

· Occasional bubbles / air pockets in optical core (“Sea Texture” Dichrolam, not Red or Green Safety glass.
· Microbubbles may be present throughout, though undetectable at two foot viewing distance.

· Occasional dust specs or foreign matter within lamination layer due to manual, “hand made” nature of the manufacture (in custom substrate cases).

· Edge fissures within ¼” from edge of air pockets at edges that may or may not show up over one to two years time.  This occurs due to “drying” of lamination adhesive at edge, and shrinkage of substrate due to off- gassing.  This is accelerated in exterior or moist conditions, but generally will not “creep” beyond ¼” from edge.  Low - solvent sealants applied to edge reduce this occurrence.  High – solvent adhesives at edge accelerate this occurrence.  Edge fissure delaminations on the “Sea Texutre” Dichrolam may creep beyond this margin, but is almost impossible to see, even upon close inspection, and does not affect visual or structural properties. 

· Color uniformity.  Transmitted and reflected colors are subject to the uniform thickness of the dichroic films used in creating these exotic laminates, and there will always be minor bands of color or intensity deviations that are impossible to prevent, as the films very high – tech and are the only ones of their kind.
All storage, handling, and final applications / mounting of any construction of JBD dichroic laminates must be protective of surfaces from scratching.  The following limitations must not be exceeded:

· Storage: Indoor, vertical or flat storage is recommended, not leaning.
· Be sure to protect edges and surfaces during transport.  Aggressive banding, strapping and tying down of sheets without corner protectors will damage sheets 

· Overtightened fastening through sheets

· Exposure of all or part of sheet (mainly plastic laminations) to extreme temperature sources like direct sunlight, hot or cold vents, or friction induced heat from poor fabrication.

APPLICATION / INSTALLATION
JBD dichroic laminates must be sufficiently supported, through encapsulation in a frame, edge only bonding, or point hold like standoffs through holes (spider fittings, etc.).  Opaque Dichrolam like the “Sea” textures should be soft bonded AT EDGES ONLY to an appropriate substrate with similar expansion / contraction coefficient.  See “Dichrolam ‘Sea’ Textures Typical Constructions” diagram. 
Templates provided to JBD for fabrication of Dichrolam must be accurate, and warranty is void if provided templates are inaccurate.   

Polycarbonate, PETG, and acrylic laminations are recommended for non-wear applications only, because of its lower resistance to surface abrasion.  Although some Dichrolam constructions are protected by a scuff-resistant coating, plastic based Dichrolam is not recommended for heavy use horizontal applications (e.g. flooring, kitchen counters, restaurant service counters, etc.).

FABRICATION
Plastic based Dichrolam: Fabrication techniques are fairly straightforward requiring tooling normally used in most plastic fabrication and cabinet shops.  Cutting/edging tools recommended:

· Plastic scoring knives (cutting through dichroic film surface excluding the “Sea series” like Black Sea, Crystal Sea and Caribbean)

· Circular saws: triple-chip grind blades are best.  Cut Dichrolam with dichroic film side of sheet facing teeth, so teeth cut through film first, backed by the plastic substrate.  Dull, or aggressive blades (fewer than 60 tooth) can create melt burrs and fragments that cause delamination bubbles over time at edges.  Always use sharp blades.  

· Band saws  (create least aggressive cutting process)

· Spiral Carbide routers/milling heads and abrasive sanding: low aggression cutting when film surface of Dichrolam is sheared in a down-shear cutting action through the film layer.  Clean bits frequently to keep from gumming up bit.

· Wet sanding and buffing edges are best method to create a polished edge.  Flame polishing is only recommended under advisement from JBD.
All frayed and delaminated film edges from cutting must be beveled down or milled off with a down-shearing cutting motion to force laminate against substrate ( manual disc or belt sanding with down motion is common to create micro bevel).  Scored edges of plastic Dichrolam require this down bevel to prevent delamination curling, which can creep into sheet excessively.  
Adhesives: Most solvent based and two part adhesives work well, with no adverse effects, as long as adhesive is not onto dichroic film surface (weak bond) – requiring film removal at glue joint.

Annealed glass based Dichrolam: Fabrication techniques are fairly straightforward requiring tooling normally used in most glass fabrication shops.  Cutting/edging tools recommended:

· Glass cutters (score and snap method): For laminated glass versions of Dichrolam, (excludes “Sea” series) cut like normal laminated glass by scoring one face with a good oiled cutter, run the split, then flip over and score and split opposite side.  Do not use flame method to melt interlayer – simply flex and run a razor to split.  Due to flexing created from this type of cutting, delamination fissuring will occur about ¼” in from the edge, therefore cut oversize and grind ¼” off. Diamond saws and waterjet cutting will eliminate this edge fissuring, and is recommended. 

· Edging: Cup wheel, peripheral wheel, flexible diamond discs, 3M Trizact polishing discs and Cerium polishing felt can be used in laminated glass Dichrolam.  “Sea” series Dichrolam requires special techniques under advisement from JBD – call for info. 

Adhesives: Limited soldering procedures are possible if method imparts least amount of heat to dichroic film face through use of shields etc.  UV Glues are best, as long as adhesive is not onto film surface (weak bond).
“Chromacrystal” three layer “shattered” FX glass laminations:

Lamination is ordered as “final size” with shape and holes specified prior to manufacturing due to tempered glass requirement, and no cutting or drilling is possible after lamination by buyer.  Flat edge polishing is available.  Adhering a metal or wood edging flush with face is common.   
Dichrolam “Black Sea”, “Caribbean”, “Red Burl” and “Crystal Sea” 

The “Sea” series of Dichrolam is commonly supplied to buyer with the dichroic textured “Sea” pattern protected inside the panel by an edge-bonded backer sheet of glass or plastic for seal and protection for installers to install like normal laminated glass or wall / table top panels.  In some applications, the Dichrolam can be supplied with a soft felt backing material without this structural backer panel for fabrication ease, cost reduction, and/or thickness restrictions.  

This unbacked version of “Sea” series Dichrolam can NEVER allow mounting bond ONTO the felt backing surface (field vs edges), only at edges or holes.  Installation can only be:

· In frames where Dichrolam panel is “floating” in the grooves or rabbet of a frame, allowing for expansion/contraction

· Sealed in a mortise – where Dichrolam surface is flush, slightly above, or below framing allowing a 3/16” ± gap to allow silicone or butyl sealant to hold panel in place at edges only.

· Fastened through holes with rubber standoff bushings inside of hole, and rubber washers at face and back at sufficient thickness clearance so fastener (screw or bolt) does not compress the Dichrolam pattern or impede expansion/contraction. 
Crystal Sea, Black Sea, Red Burl, and Caribbean are designed primarily as wall tiles, table/bar tops and inlays where the clear glass or plastic face is exposed, not the textured film/felt back.  This means that the textured side with the felt backer is NOT designed for bonding to substrate with ANY adhesive – must be dry mount where bonding is at edges only such as grout in tile application, groove of frame, or silicone flush set at edges (tabletops) as explained earlier in “Application / Installation”.  Dichrolam “Sea Textures” specified with exposed polished edges will be supplied with a backing panel identical to face panel with a 3/16” to ½” wide seal margin at full perimeter, with seal thickness of 3/32” to 1/8” thick, depending upon pattern/color.  Crystal Sea edge seals are created with crystal clear sealants, Black Sea and Red Burl use black opaque sealants and Caribbean uses white or black sealants.  Typical edging is flat polish with polished arris (micro bevel chamfer) on top edge.  All cold-forming is risk of buyer – delamination possible due to shear.  All applications should be approved by this office, as Dichrolam is a unique material with unique limitations.  

MAINTENANCE
Surfaces should be cleaned using a clean, soft cotton cloth  with normal glass cleaners. Isopropyl alcohol is strongest solvent recommended for plastic based Dichrolam – no MEK, acetone or similar solvents.  Abrasive cleaners, strong ammonia or alkaline solutions should always be avoided unless glass based products are used.

SIZE AVAILABILITY, COLOR AND COST
Available in lengths up to 120 inches x 48” wide and cut to specified size lists (as well as special order extended lengths / widths for all products other than Red and Green safety glass).  Widths of 53” are possible upon request.   

· Colors are “Red” and “Green” for the flat, non-textured laminated glass Dichrolam, as well as Crystal Sea “Red” and “Green”.  Color spec is based on reflection color at perpendicular viewing with dark background, and transmitted color is always complimentary (opposite) to reflected color – all the way through the color shift.  

· Transmission color for “Red” at right angle viewing will be aqua blue/green, shifting through deep blue, then magenta at skew angle viewing, while reflection color will be copper / red shifting through yellow / gold and into green at skew angles.

· Transmission color for “Green” at right angle viewing will be magenta / purple, shifting through orange, then yellow at skew angle viewing, while reflection color will be green shifting into deep blue at skew angles.

· Caribbean has a white, opaque backing, and exhibits the teal and coral colors of the Caribbean. 

· Black Sea Dichrolam has a black, opaque backing and shows blue, green, violet and “veining” of copper and yellow streaks. 

· Red Burl is similar to Black Sea but with copper red and green reflections with dark and sometimes purple “veining” and streaking .

All costs are by custom quote only, although it is roughly 50% of the cost of common dichroic glass.  Call authorized representative.  

TECHNICAL SERVICE
For technical service, please contact John Blazy at 216 749 0692. 
DICHROLAM LIMITATION OF WARRANTY & LIABILITY

	Seller warrants that the products sold hereunder shall be of merchantable quality and shall conform in all material respects to Seller’s standard specifications shown herein.  Buyer assumes all risks as to the results of the use of the products purchased, whether used singly or in combination with other materials or in any process.  Manufacturers who resell Dichrolam as their own products to third and fourth party etc. users forfeit all warranty rights due to original manufacturer’s (JBD) loss of control over final engineering, application, fabrication, and installation specifics.

Limitations of Claims

At Seller’s option, Seller will replace, without additional charge, products which do not comply with the warranty or, upon return of the products at Seller’s expense, refund the purchase price up to three full years from date products are received by buyer.  Reinstallation of replacement products are at buyers expense unless due to breach of warranty or as otherwise noted.
SELLER MAKES NO WARRANTY, EXPRESS OR IMPLIED, BASED ON ANY COURSE OF DEALING OR USAGE OF TRADE OR OF FITNESS FOR PARTICULAR USE OR OTHER-WISE, OTHER THAN THAT STATED HEREIN OR REQUIRED BY APPLICABLE LAW.   SELLER’S LIABILITY FOR ANY LOSS OR CLAIM WHATSOEVER, INCLUDING A CLAIM FOR BREACH OF THE WARRANTY OF MERCHANTABILITY, SHALL BE LIMITED SOLELY AND EXCLUSIVELY TO REPLACEMENT OF DEFECTIVE OR NON-CONFORMING PRODUCTS OR, AT THE ELECTION OF SELLER, TO RETURN OF THE PRODUCTS AND REPAYMENT OF THE PURCHASE PRICE. IN NO EVENT SHALL SELLER BE LIABLE FOR ANY OTHER ACTUAL DAMAGE OR EXEMPLARY DAMAGES.

Any course of dealings between the parties to the contrary notwithstanding, buyer is responsible for inspection of the product upon receipt and prior to any cutting, fabrication, or installation.  Any claim by Buyer for breach of warranty shall be deemed waived to the extent it could have  been  determined  by  such  inspection, unless presented in writing to the Seller within thirty (30) days from the date of receipt of the products to which such claim relates.  In all events, such claims not made within two months after receipt are deemed waived.

	Some products are shipped with a protective film to protect product during transit and storage.  All such products must be inspected for defects prior to cutting, fabrication, or installing.  Surface must then be protected during cutting, fabrication, and installation.  Failure to remove the protective film to inspect for defects prior to cutting or fabrication is at Buyer’s risk.

Seller shall have no liability for defects or other failures caused by failure to fabricate, install, use or maintain the products in accordance with John Blazy Designs’ instructions or damage to product occurring after shipment to the initial purchaser.

Buyer assumes all risk and liability for loss, damage or injury to the person or property of Buyer or others arising out of use or possession of any products sold hereunder.  Any questions concerning this warranty or requests for service should be to: John Blazy Designs Attn:  John Blazy.








PAGE  
2

