ALTRO LAVENCIA PLUS

Vinyl Tile

SECTION 09657

RESILIENT Vinyl Flooring

(Tile Flooring)

PART 1 	GENERAL

1.01	SUMMARY

A.	This Section includes: Heavy duty luxury vinyl tile flooring.

B.	Conform with requirements of all Sections of Division 1, General Requirements, as it applies to the work of this Section.

1.02	RELATED SECTIONS

A.	Section(s) related to this Section include:

1.	Concrete: Division 3.

2.	Wood & Plastics: Division 6.

3.	Thermal & Moisture Protection: Division 7.

4.	Mechanical: Division 15.

1.03	REFERENCES

A.	General: Standards listed by reference, including revisions by issuing authority, form a part of this specification section to extent indicated. Standards listed are identified by issuing authority, authority abbreviation, designation number, title or other designation established by issuing authority. Standards subsequently referenced herein are referred to by issuing authority abbreviation and standard designation.

B.	American Society for Testing & Materials (ASTM):

1.	ASTM D2047 Standard Test Method for Static Coefficient of Friction of Polish-Coated Floor Surfaces as Measured by the James Machine.

2.	ASTM E648 Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

3.	ASTM E84 Flame Spread

C.	Resilient Floor Covering Institute (RFCI)

1.	RFCI Standard Slab Moisture Test Method (Calcium Chloride Method).

1.04	SUBMITTALS

A.	General: Submit listed submittals in accordance with Conditions of the Contract and Division 1 Submittal Procedures Section.

B.	Product Data: Submit product data, including manufacturer’s information, for specified products.

C.	Shop Drawings: Submit shop drawings showing layout, profiles and product components, including drain details, accessories, finish colors, patterns and textures.

D.	Samples: Submit selection and verification samples for finishes, colors and textures.

E.	Quality Assurance Submittals: Submit the following:

1.	Test Reports: Certified test reports showing compliance with specified performance characteristics and physical properties.

2.	Manufacturer’s Instructions: Current published manufacturer’s installation and maintenance instructions.

- Manufacturer’s Field Reports: Manufacturer’s field reports specified herein.

F.	Closeout Submittals: Submit the following:

1.	Operation and Maintenance Data: Operation and maintenance data for installed products in accordance with Division 1. Include methods for maintaining installed products and precautions against cleaning materials and methods detrimental to finishes and performance.

2.	Warranty: Warranty documents specified herein.

1.05	QUALITY ASSURANCE

- Installer Qualifications: Experienced in performing work of this section and who is specialized in the installation of work similar to that required for this project. Installation of Altro Lavencia Tile should follow the instructions detailed in the Altro Lavencia Tile Installation Guide.

1.	Training: Installer who has attended an Altro installation training clinic.

B.	Mock-ups: Install at project site a job mock-up using acceptable products and manufacturer approved installation methods, including concrete substrate testing. Obtain Owner’s and Consultant’s acceptance of finish color, texture and pattern, and workmanship standards.

1.	Mock-up Size: [Specify mock-up size.].

2.	Maintenance: Maintain mock-up during construction for workmanship comparison; remove and legally dispose of mock-up when no longer required.

3.	Incorporation: Mock-up may be incorporated into final construction upon Owner’s approval.

C.	Pre-installation Meeting: Conduct pre-installation meeting to verify project requirements, substrate conditions, manufacturer’s installation instructions and manufacturer’s warranty requirements.

1.06	DELIVERY, STORAGE & HANDLING

A.	Ordering: Comply with manufacturer’s ordering instructions and lead time requirements to avoid construction delays.

B.	Deliver materials in manufacturer’s original, unopened, undamaged containers with identification labels intact.

C.	Store materials protected from exposure to harmful weather conditions, at temperature and humidity conditions recommended by manufacturer.

1.07	PROJECT CONDITIONS

A.	Temperature Requirements: If storage temperature is below 68F (20C), move the Altro Lavencia Tile to a warmer place and allow to reach this temperature before installation. Maintain temperature of installation area between 68F (20C) and 80F (26C) for a period of at least 72 hours prior to, during, and after completion of the installation for acrylic adhesives (12 hours after completion for polyurethane adhesives).

1.08	WARRANTY

A.	Project Warranty: Refer to Conditions of the Contract for project warranty provisions.

B.	Manufacturer’s Warranty: Submit, for Owner’s acceptance, manufacturer’s standard warranty document executed by authorized company official. Manufacturer’s warranty is in addition to, and not a limitation of, other rights Owner may have under Contract Documents.

1.	Warranty Period: 20 year commercial and Llifetime residential commencing on Date of Substantial Completion.

PART 2	 PRODUCTS

2.01	FLOORING

# A.	Vinyl Tile Manufacturer: Lavencia by Altro, Telephone 800.377.5597, Fax 610.746.4325; E-Mail Assistance: support@altrofloors.com

# B. 	22 mil wear layer

# C.	Acceptable material: Altro Lavencia (measurements and product weights given below are approximate):

COLORS

- LACP99055H Tavern Tobacco: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LAFP13011R Chateau Nordic: Size: 10” x 60” Plank (254 mm x 1524 mm); Feet Per Carton: 33.33 sq. ft. (3.1 sq.mtr.); Weight Per Carton: 37.74 lbs. (15.3 kg); 8 Pieces Per Carton

- LACP55077T Persimmon: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LAFP13066R Farmhouse Whiskey: Size: 10” x 60” Plank (254 mm x 1524 mm); Feet Per Carton: 33.33 sq. ft. (3.1 sq.mtr.); Weight Per Carton: 37.74 lbs. (15.3 kg); 8 Pieces Per Carton

- LAFP13077R Farmhouse Smoke: Size: 10” x 60” Plank (254 mm x 1524 mm); Feet Per Carton: 33.33 sq. ft. (3.1 sq.mtr.); Weight Per Carton: 37.74 lbs. (15.3 kg); 8 Pieces Per Carton

- LACP88033T Country Hickory: Size: 4” x 36” Plank (101.6 mm x 914.4 mm); Feet Per Carton: 20 sq. ft. (1.85 sq.mtr.); Weight Per Carton: 23 lbs. (10.1 kg); 20 Pieces Per Carton

- LACP23066R Hampton Greige: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LAFP13033R Chateau Saddle: Size: 10” x 60” Plank (254 mm x 1524 mm); Feet Per Carton: 33.33 sq. ft. (3.1 sq.mtr.); Weight Per Carton: 37.74 lbs. (15.3 kg); 8 Pieces Per Carton

- LACP88088T Carolina Spalted Cherry: Size: 4” x 36” Plank (101.6 mm x 914.4 mm); Feet Per Carton: 20 sq. ft. (1.85 sq.mtr.); Weight Per Carton: 23 lbs. (10.1 kg); 20 Pieces Per Carton

- LACP88066T Antique Burled Oak: Size: 4” x 36” Plank (101.6 mm x 914.4 mm); Feet Per Carton: 20 sq. ft. (1.85 sq.mtr.); Weight Per Carton: 23 lbs. (10.1 kg); 20 Pieces Per Carton

- LACP88044T African Mahogany: Size: 4” x 36” Plank (101.6 mm x 914.4 mm); Feet Per Carton: 20 sq. ft. (1.85 sq.mtr.); Weight Per Carton: 23 lbs. (10.1 kg); 20 Pieces Per Carton

- LAFP13022R Chateau Cellar: Size: 10” x 60” Plank (254 mm x 1524 mm); Feet Per Carton: 33.33 sq. ft. (3.1 sq.mtr.); Weight Per Carton: 37.74 lbs. (15.3 kg); 8 Pieces Per Carton

- LAFP13055R Chateau Barrel: Size: 10” x 60” Plank (254 mm x 1524 mm); Feet Per Carton: 33.33 sq. ft. (3.1 sq.mtr.); Weight Per Carton: 37.74 lbs. (15.3 kg); 8 Pieces Per Carton

- LACP99088H Tavern Bourbon: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP55088H Tavern Mesquite: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP99077H Vintage Walnut: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP99033H Roasted Chestnut: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LASP66099R Heritage Wrought Iron: Size: 6” x 36” Plank (186.94 mm x 914 mm); Feet Per Carton: 24 sq. ft. (2.23 sq.mtr.); Weight Per Carton: 27.09 lbs. (12.3 kg); 16 Pieces Per Carton

- LACP88022T American Walnut: Size: 4” x 36” Plank (101.6 mm x 914.4 mm); Feet Per Carton: 20 sq. ft. (1.85 sq.mtr.); Weight Per Carton: 23 lbs. (10.1 kg); 20 Pieces Per Carton

- LACP99066H Malabar Blackwood: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP88033T Country Hickory: Size: 4” x 36” Plank (101.6 mm x 914.4 mm); Feet Per Carton: 20 sq. ft. (1.85 sq.mtr.); Weight Per Carton: 23 lbs. (10.1 kg); 20 Pieces Per Carton

- LACP23088H Frontier: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP 99022R Hampton Shores: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP88011T Laurel Oak: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP 23022T Northern Birch: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP88077R Oak Butternut: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP23077R Oxford Oak: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP 23055H Silver Maple: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LACP 23099H Vintage Keg: Size: 7.36” x 48.3” Plank (186.94 mm x 1226.82 mm); Feet Per Carton: 29.64 sq. ft. (2.75 sq.mtr.); Weight Per Carton: 33.44 lbs. (15.2 kg); 12 Pieces Per Carton

- LAST23033S Bisque: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST23011S Oyster: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST23044S Pewter: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST33022S Grasscloth Linen: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST33033S Grasscloth Tweed: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST33066S Grasscloth Mohair: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44011S Seagrass Yellow: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44022S Seagrass Orange: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44033S Seagrass Red: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44044S Seagrass Green: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44055S Seagrass Blue: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST33077T Moonstruck Taupe: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST33055T Mesa Cloud: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44066T Mesa Cinder: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44077T Mesa Sand: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44088T Mesa Umber: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

- LAST44099T Forge Burnished: Size: 12” x 24” Tile (304.8 mm x 609.6 mm); Feet Per Carton: 32 sq. ft. (2.9 sq.mtr.); Weight Per Carton: 36.05 lbs. (16.35 kg); 16 Pieces Per Carton

2.02	ACCESSORIES

A.	Proprietary Accessory Products: Provide Altro accessories for use with Altro Lavencia Tile:

1.	Acrylic Adhesive: Ecofix 25 for adhering flooring to substrate.

B.	Proprietary Product(s) Standard and Testing:

1.	Fire Resistance: Flammability exceed minimum for Class 1 rating per ASTM E648.

2.	Smoke Density: Less than 450 when tested in accordance with ASTM E662.

2.03	PRODUCT SUBSTITUTIONS

A.	Substitutions: No substitutions permitted.

2.04	SOURCE QUALITY

  - Source Quality: Obtain flooring products from a single manufacturer.

2.05 	ADHESIVES

1. Altrofix 30- 2 part polyurethane for areas prone to moisture

PART 3	 EXECUTION

3.01	MANUFACTURER’S INSTRUCTIONS

A.	Compliance: Comply with manufacturer’s product data, including product technical bulletins, product catalog, installation instructions and product label instructions for installation.

3.02	EXAMINATION

    - Site Verification of Conditions: Verify substrate conditions, which have been previously installed under other sections, are acceptable for product installation in accordance with manufacturer’s instructions.

3.03	PREPARATION

A.	Lavencia Tile flooring shall be installed over subfloors conforming to ASTM F710 for concrete and other monolithic floors or ASTM F1482 for wood subfloors.

B.	Moisture Testing: Moisture emissions from concrete subfloors must not exceed 5 lbs per 1000sf per 24 hours (2.25 kg H2O/24 hr/93 m2) via the Calcium Chloride Test Method (ASTM F1869) and not to exceed 85% internal concrete relative humidity as tested in accordance with ASTM F2170-02. If subfloor moisture exceeds the allowable maximum for installing Altro Lavencia Tile, please call your local Altro distributor for advice.

C.	Wood subfloors shall not exceed 10% moisture content when measured with a Delmhorst Wood Moisture Tester.

D.	The pH level of the subfloor surface shall not be higher than 9.9.  If higher, subfloor must be neutralized.

- Underlayment and Patching Compounds: Use only gray colored Portland cement based underlayments; patching compounds are used for filling cracks, holes and leveling. White gypsum materials are not acceptable.

3.04	INSTALLATION

A.	Lavencia Tile Installation: Install Altro Lavencia Tile in accordance with the current published Altro Installation Guide. Failure to install Altro Lavencia Tile in accordance with recommended procedures will void the Altro Limited Product Warranty.

3.05	FIELD QUALITY REQUIREMENTS

A.	Manufacturer’s Field Services: Upon Owner’s request, provide manufacturer’s field service consisting of product use recommendations and periodic site visits for inspection of product installation in accordance with manufacturer’s instructions.

1.	Site Visits: [Specify number and duration of periodic site visits.].

3.06	CLEANING

A.	Cleaning: Remove temporary coverings and protection of adjacent work areas. Repair or replace damaged installed products. Clean installed products in accordance with manufacturer’s instructions prior to Owner’s acceptance. Remove construction debris from project site and legally dispose of debris.

3.07	PROTECTION

A.	Protection:

    - Protect the newly installed flooring from foot traffic for 24 hours and heavy rolling traffic for 72 hours.

2.	Protect installed product and finish surfaces from damage during construction.

B.	Cover and protect finished installation from damage that may be caused by other trades using a plywood or non-staining temporary floor protection system, such as textured plastic sheeting.

-------------------------------------------------------END OF SECTION-----------------------------------------------------------