Division 06 61 00

BioPrism® SOLID SURFACE
TRENCH RECEPTOR

PART 1 – GENERAL

1.01 SUMMARY

A. Shower Receptors

1.02 SECTION INCLUDES

A. Solid Surface Trench Receptors

1.03 REFERENCES

A. American National Standards Institute (ANSI)

1.04 SYSTEM DESCRIPTION

A. Performance Requirements: Provide shower receptors that conform to the following requirements of regulatory agencies and the quality control of Inpro® Corporation.

1. Provide shower receptors that conform to ANSI124.1.2-2005 when tested for workmanship and finish, structural integrity and material characteristics.

2. Provide Shower receptors that conform to ANSI Z457/CSA B45.5-11 when tested for load bearing.

1.05 SUBMITTALS

A. Product Data: Manufacturer's printed product data for each type of shower receptor specified.

B. Samples: Verification samples minimum of 1 ½” x 3" samples indicating color.

C. Manufacturer's Installation Instruction: Printed installation instructions for shower receptors.

1.06 DELIVERY, STORAGE AND HANDLING

A. Deliver materials in unopened factory packaging to the jobsite

B. Inspect materials at delivery to assure that specified products have been received.

C. Store in original packaging in an interior climate controlled location away from direct sunlight.

1.07 PROJECT CONDITIONS

A. Environmental Requirements: Products must be installed in an interior climate controlled environment.

1.08 WARRANTY

A. Standard BioPrism® Solid Surface Limited 10 Year Warranty against material and manufacturing defects.

PART 2 – PRODUCTS

2.01 MANUFACTURER

A. Acceptable Manufacturer: 


Inpro® Corporation
PO Box 406 Muskego, WI 53150 USA

Telephone: 800.222.5556, Fax: 888.715.8407,

www.inprocorp.com

B. Substitutions: Not permitted

C. Provide all shower receptors from a single source.

2.02 MANUFACTURED UNITS

A. BioPrism® Solid Surface Trench Receptors

1. Width of Trench receptor shall be 37 ½”, 49 ¾”, 61 ¾”, and 73 ¾” outside dimension, standard; custom widths up to 73 ¾” available.
2. Depth of Trench Receptor shall be customizable with a minimum of 32" and maximum of 48 ¾”” outside dimension.

3. Drain Location shall be 4 15/16” on center from the front edge of the receptor. Minimum drain offset from either edge varies by size.
4. Water barrier shall be BioPrism® Solid Surface, Dimensions: ½” thick x 4 ½” tall measuring height at the outside of the shower receptor (inside height may vary based on overall depth of the receptor)
5. Flange shall be BioPrism® Solid Surface, Dimensions: ¼” thick x 5" Tall measuring height at the outside of the shower receptor (inside height may vary based on overall depth of the receptor).

6. Opening condition shall be roll-in (3/4” front edge thickness) 
7. Optional ¼” Thick Add-on Threshold
B. Shower Drain:

1. Trench Grate: Trench grate shall be 12 gauge brushed stainless steel with weep holes
a. Secured with stainless steel tamper resistant fasteners. (Standard)
b. Secured with magnetic fastening system.
2. Shower drain shall be Oatey number 42150, Brass, No-calk, Drain. Drain body is sealed to shower base with a fiber and rubber washer. Drain is secured to 2”, 40 DWV pipe with a mechanically compressed gasket that does not require caulking.

2.03 MATERIALS
A. BioPrism® Solid Surface: Trench Receptor shall be manufactured from a bio-based, polyester modified, acrylic hybrid resin.
2.04 FINISHES
A. Select color from InPro® Corporation BioPrism® Solid Surface Shower Systems color palette.
PART 3 – EXECUTION
3.01 EXAMINATION
A. Examine areas and conditions in which shower receptors will be installed.
3.02 PREPARATION
A. General: Prior to installation, clean area to remove dust, debris and loose particles.
3.03 INSTALLATION
A. General: Install components plumb and level, scribe adjacent finishes, in accordance with approved shop drawings and recommended installation instructions.
3.04 CLEANING
A. At completion of the installation, clean surfaces in accordance with the Inpro® BioPrism® Solid Surface clean-up and maintenance instructions.

END OF SECTION

IPC.1998/Rev.5

[image: image1]

[image: image1]