SECTION 092900 – Gypsum Board, 1/2 in. and 5/8 in. USG Sheetrock® Brand Glass-Mat Panels Mold Tough® (Regular and Firecode® X)

Product Summary:

- High-performance interior wall panels with moisture and mold resistance. - Suitable for use in pre-dry-in (aka “pre-rock”) and similar applications of wallboard before the building envelope is fully enclosed. - For use in interior applications where glass-mat gypsum panels are desired. - Features an inorganic fiberglass face and back. - Can be used in protected exterior soffit applications - Scores and snaps easily for quick installation - Installs and finishes similar to standard drywall - UL Classified as to fire resistance, surface-burning characteristics and noncombustibility - For more information, contact USG at 800.874.4968 for technical questions.

Note to Specification Writer:

- This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections: 09 29 00 – GYPSUM BOARD. - This product will be produced at USG gypsum board plants, substantially reducing distances and carbon footprint for transport. - For more information, reference product submittal sheet WB2981 and usg.com.

PART 2 –PRODUCTS

GYPSUM BOARD – TYPE X, MOISTURE RESISTANT

Glass-Mat Interior Gypsum Board, Type X: ASTM C1658/C1658M. With fiberglass mat laminated to both sides.  Designed for interior use.

Basis of Design: Subject to compliance with project requirements, the design is based on the following: United States Gypsum Company, LLC, “USG Sheetrock® Brand UltraLight Panels Mold Tough® Firecode® X”.

Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

UL Classification / core thickness: [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type SGX].

ASTM E136: Non-combustible gypsum core.

ASTM E84 Surface-Burning Characteristics:

Flame Spread: 0.

Smoke Developed: 0.

ASTM D3273 Mold Resistance: A score of 10 as rated according to ASTM D3273.

Length: [8′-0″ (2440 mm)] [9′-0″ (2732 mm)] [10′-0″ (3050 mm)] [12′-0″ (3660 mm)].

Width: 4’-0″ (1219 mm).

Weight: [1/2” thick board 2.0 lbs./ft2.] [5/8” thick 2.4 lbs./ft2.]

Long Edges: Tapered.

Disclaimer: The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project. These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.