SECTION 09 06 48 - CORK FLOORING

- GENERAL

  - SUMMARY

    - SECTION INCLUDES:

      - Cork floor tile

      - Adhesives

      - Finishes

    - RELATED SECTIONS

      - Section 03300 - Cast-In-Place Concrete Floor substrate requirements.

      - Section 06200 - Rough Carpentry:  Floor substrate requirements.

  - REFERENCES

    - American Concrete Institute (ACI):

      - ACI 302.2R - Guide for Concrete Slabs that Receive Moisture-Sensitive Flooring Materials

    - American Society for Testing and Materials (ASTM):

      - ASTM E648 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

      - ASTM E662 - Standard Test Method for Specific Optical Density of Smoke Generated by Solid Materials.

      - ASTM F137 - Standard Test Method for Flexibility of Resilient Flooring Materials with Cylindrical Mandrel Apparatus.

      - ASTM F141 - Standard Terminology Relating to Resilient Floor Coverings

      - ASTM F386 – Standard Test Method for Thickness of Resilient Flooring Materials Having Flat Surfaces

      - ASTM F710 - Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring.

      - ASTM F925 - Standard Test Method for Resistance to Chemicals of Resilient Flooring.

      - ASTM F970 - Standard Test Method for Static Load Limit.

      - ASTM F1482 – Standard Practice for Installation and Preparation of Panel Type Underlayments to Receive Resilient Flooring.

      - ASTM F1869 -  Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride

      - ASTM F1914 - Standard Test Methods for Short-Term Indentation and Residual Indentation of Resilient Floor Covering.

      - ASTM F2055 – Standard Test Method for Size and Squareness of Resilient Floor Tile

      - ASTM F2199 - Standard Test Method for Determining Dimensional Stability of Resilient Floor Tile after Exposure to Heat.

      - ASTM F3008 – Standard Specification for Cork Floor Tile

    - State of California (CA)

      - CA Section 01350 – Special Environmental Requirements (Indoor Air Quality)

    - California Department of Public Health (CDPH)

      - CDPH Standard Method v 1.2 - Standard Method for Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers

    - California High Performance Schools (CHPS)

      - CHPS Section 01350 - Low-Emitting Materials Criteria for Use in Classrooms.

    - Declare™

      - Product material disclosure labeling program.

    - International Organization for Standardization (ISO)

      - ISO 4918 – Resilient, Textile and Laminate Floor Coverings – Castor Chair Test

    - Living Building Challenge (LBC)

      - LBC Chemical Red List Version 3.1.

    - National Fire Protection Association (NFPA)

      - NFPA 80 – Fire Safety Code.

      - NFPA 253 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

      - NFPA 255 - Standard Test Method for Surface Burning Characteristics of Building Materials.

    - Resilient Floor Covering Institute (RFCI)

      - Recommended Work Practices for Removal of Resilient Floor Coverings

    - Underwriters Laboratories (UL) Environment

      - UL 410 – Slip Resistance of Floor Surface Materials

      - Certified Body of GreenGuard Gold Indoor Air Quality / VOC Emissions Certification.

  - SUBMITTALS

    - General: Submittals must be submitted the under provisions of Section 01300.

    - Product Data:  Manufacturer's published documents on each product to be used, including:

      - Storage and handling requirements.

      - Installation instructions and initial maintenance instructions per Technical Data Sheets.

      - Maintenance and initial finish application instructions per Care & Maintenance documents.

    - Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

    - Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (150 mm) square or one full tile, representing actual product, color, and patterns.

  - SUSTAINABILITY REQUIREMENTS

    - CA Section 01350 / CHPS Section 01350

        - Provide building materials that comply with CA Section 01350 and CHPS Section 01350 when tested in accordance with CDPH Standard Method v 1.2.

        - Provide test data or third party certification that confirms compliance.

    - LBC Chemical Red List 3.1

        - Provide building materials that are Red List Free in accordance the LBC Chemical Red List 3.1.

        - Provide full material disclosure or third party certification that confirms compliance.

  - QUALITY ASSURANCE

    - Cork Tile

      - Cork tile is a natural product – as such, shade and color variations are inherent.

    - Qualifications:

      - Installer Qualifications: Installer must be a professional, licensed and experienced installer. Installer must have familiarity with both the type, size and format of the product.

      - Manufacturer’s Qualifications: Manufacturer must provide remote and field technical support and service prior to, during and following installation, as necessary.

    - Mock-Up:

      - Provide a mock-up for evaluation of product, surface preparation techniques and installation workmanship.

      - Do not proceed with remaining work until size, color, thickness, sheen and workmanship are approved by Architect, End-User and/or other stakeholders.

      - Maintain mock-up area as required in accordance with Care & Maintenance documents to produce acceptable work.

  - DELIVERY HANDLING & STORAGE

    - Ordering: Comply with manufacturer’s ordering and lead time requirements to avoid construction delays.

    - Storage: Store products in climate controlled space (65° F (19° C) - 85° F (30° C), 45% - 55% RH) for at least 72 hours prior to installation. Keep products in manufacturer's unopened packaging until ready for installation (except for rolled goods).

    - Acclimation: Rolled goods must be unrolled and allowed to relax and acclimate for 24 hours prior to installation.

  - PROJECT CONDITIONS

      - Environmental Conditions: Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer in accordance with product technical data sheets.  Do not install products under environmental conditions outside manufacturer's absolute limits.

    - WARRANTY

      - Project Warranty: Refer to Conditions of Contract for project warranty provisions.

      - Manufacturer’s Commercial Warranty: Mediterra 2.0 shall be warranted for ten years for material or manufacture defects.

- PRODUCTS

  - PRODUCT MANUFACTURERS

    - Acceptable Manufacturer:

      - Capri Collections

215 Bucky Drive

Lititz, PA  17543

P: 800.492.2613 
E: sales@capricollections.com

Web: www.capricollections.com

  - SUBSTITUTIONS

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 01 section on product options and substitutions.

    - Substitutions:  Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Division 01.

  - PRODUCT DIMENSIONS

** NOTE TO SPECIFIER ** Delete sizes not required.

    - Product: Capri Mediterra 2.0 Cork Tile as manufactured by Capri Collections.

Standard Sizes

      - 12 inches by 24 inches by 3/16 inch (305 mm by 610 mm by 4.8 mm).* All STANDARD colors.

      - 12 inches by 12 inches by 3/16 inch (305 mm by 305 mm by 4.8 mm) Standard colors: Light, Medium, Dark, Blocks, Cable, Dark, Light, Tumbled.

Non-Standard Sizes (1080 sf minimum per color and lead time will apply)

      - 12 inches by 12 inches by 3/16 inch (305 mm by 305 mm by 4.8 mm) All colors other than Blocks, Cable, Dark, Light, Medium, Tumbled.

      - 24 inches by 24 inches by 3/16 inch (610 mm by 610 mm by 4.8 mm)

      - 5.91 inches by 23.62 inches by 3/16 inch (150 mm by 600 mm by 4.8 mm)

      - 11.81 inches by 35.43 inches by 3/16 inch (300 mm by 900 mm by 4.8 mm)

      - 12 inches by 12 inches by 5/32 inch (305 mm by 305 mm by 4 mm)

      - 12 inches by 24 inches by 5/32 inch (305 mm by 610 mm by 4 mm)

      - 11.81 inches by 35.43 inches by 5/32 inch (300 mm by 900 mm by 4 mm)

      - 12 inches by 12 inches by 5/16 inch (305 mm by 305 mm by 8 mm)

      - 12 inches by 24 inches by 5/16 inch (305 mm by 610 mm by 8 mm)

      - 24 inches by 24 inches by 5/16 inch (610 mm by 610 mm by 8 mm)

      - 5.91 inches by 23.62 inches by 5/16 inch (150 mm by 600 mm by 8 mm

      - 11.81 inches by 35.43 inches by 5/16 inch (300 mm by 900 mm by 8 mm)

  - PRODUCT COLORS 
              ** NOTE TO SPECIFIER ** Delete colors not required.

Standard Colors

      - Acorn GD2655C

      - Anchor GD2652C

      - Blocks GD2606V

      - Cable GD2607V

      - Chestnut GD2656C

      - Dark GD2602H

      - Jumble GD2604H

      - Light GD2600H

      - Maize GD2654C

      - Medium GD2601V

      - Olive GD2658C

      - Pick-Up Strips Light GD2603H

      - Platinum GD2651C

      - Rapids GD2653C

      - Sea Salt GD2650C

      - Small Strips GD2605H

      - Taupe GD2657C

      - Tea Leaves GD2659C

      - Tumbled GD2608V

Non-Standard Colors (1080 sf minimum per color and lead time will apply)

      - 2Stuco GD2609V

      - Cabernet GD2660C

      - Dark Tracks GD2611H

      - Fresco GD2618H

      - Light Tracks GD2614H

      - Mélange GD2610H

      - Mulch GD2613V

      - Pathways GD2615V

      - Pick Up Strips Dark GD2616H

      - Port GD2621C

      - Rosewood GD2662

      - Sunset GD2663C

      - Terrain GD2612H

      - Billows Ash GD3545

      - Billows Brown GD3540

      - Billows Current GD3590

      - Billows Ore GD3575

      - Broken Lines GD3575

      - Channel GD3565

      - Channel White GD3570

      - ECC Chestnut GD3550

      - Gray Wash GD3580

      - Plateau GD3501

      - Rugged GD3505

      - Sable GD3595

*H = Homogeneous / V = Veneer / C = Colours

  - PHYSICAL CHARACTERISTICS

    - ASTM F3008 – Cork Tile

      - EN 434 – Curling: Passes, <6mm

      - ASTM F137 – Flexibility: Passes

      - ISO 4918 – Castor Chair Test - Passes

      - ASTM F970 – Static Load Limit: Passes, 250 lbs.

      - ASTM F1914 – Residual Indentation: Passes, <8%

      - ASTM F2199 – Dimensional Stability: Passes, <0.05 in. change

      - ASTM F925 – Chemical Resistance:

        - White vinegar (5% Acetic Acid) - Passes.

        - Rubbing Alcohol (70% Isopropyl Alcohol) - Passes.

        - Lye (5% Sodium Hydroxide) - Passes.

        - Hydrochloric Acid (5% HCI) - Passes.

        - Sulfuric Acid (5%H2SO4) - Passes.

        - Household Ammonia (5% Ammonia) - Passes.

        - Disinfectant Cleaner (5% Active Phenol) - Passes.

        - Household Bleach (5.25% NaOCl) - Passes.

        - Unleaded Gasoline - Passes.

        - Kerosene - Passes.

        - Olive Oil - Passes.

    - ASTM E648 (NFPA 253) – Class II, 0.22-0.44 W/cm2

    - ASTM E662 (NFPA 258) – Smoke Density: Passes, <450

    - UL 410 – Slip Resistance: >0.7 (wet), >0.5 (dry)

  - ACCESSORIES

    - Matching and compatible moldings and accessories are available through Capri Collections.

  - PRODUCT FINISH

** NOTE TO SPECIFIER ** Delete if not required.

    - Only Capri Collections approved floor finishes shall be used when installing Mediterra 2.0.

      - Site-Applied Urethane Finish: Loba 2K Supra AT Satin.

  - PRODUCT ADHESIVE

** NOTE TO SPECIFIER ** Adhesive is not optional.

    - Only Capri Collections approved adhesives shall be used when installing Mediterra 2.0.

      - Gold Series WC 1000 Water-Based Cork Contact Adhesive

- EXECUTION

** NOTE TO SPECIFIER ** Revise articles below to suit specific project requirements.

  - MANUFACTURERS INSTRUCTIONS

    - Compliance: Review and comply with manufacturer’s technical data sheets, care & maintenance documents, warranty information, technical bulletins and written specifications.

  - EXAMINATION

    - Site Verification of Conditions:

      - Verify substrate conditions, which have been previously installed under other sections, are acceptable for product installation in accordance with manufacturer’s technical data.

      - Do not begin installation until all substrates have been properly tested and prepared in accordance with Capri Mediterra 2.0 technical data sheets and applicable ASTM, ACI, NWFA and RFCI standards.

      - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Cleaning: Clean surfaces thoroughly prior to installation.

    - Substrate Preparation: Prepare surfaces in accordance with substrate preparation requirements published in Capri Mediterra 2.0 technical data sheets.

  - INSTALLATION

    - Flooring Installation: Install materials in accordance with installation instructions published in Capri Mediterra 2.0 technical data sheets.

    - Traffic Limits: No traffic, cleaning, finishing or placement of furniture should occur in accordance with adhesive traffic limits published in adhesive technical data.

    - Initial Maintenance: Once traffic limits have lapsed, perform initial maintenance in accordance with initial maintenance instructions published in Capri Mediterra 2.0 technical data sheets and care & maintenance documents.

  - FINISH APPLICATION

    - Initial Maintenance: Ensure surfaces have had initial maintenance performed in accordance with initial maintenance instructions published in Capri Mediterra 2.0 technical data sheets and care & maintenance documents.

    - Cleaning: Clean surfaces thoroughly prior to finish application.

    - Finish Application: Install finish in accordance with initial finish application instructions published in Capri Mediterra 2.0 technical data sheets and care & maintenance documents.

  - MAINTENANCE

    - Daily Maintenance: Long-term care and maintenance must be performed in accordance with daily and routine maintenance instructions published in Capri Mediterra 2.0 care & maintenance documents.

    - Finish Reapplication: Site-applied finish that is improperly applied or damaged may require finish re-application in accordance with finish removal and reapplication instructions published in Capri Mediterra 2.0 care & maintenance documents.

  - PROTECTION

    - Temporary Floor Protection: Protect installed products until completion of project in accordance with flooring or material protection requirements published in Capri Mediterra 2.0 technical data sheets and care & maintenance documents.

    - Repair: Touch-up, repair or replace damaged products prior to Substantial Completion.

    - Permanent Floor Protection: Ensure furniture feet/bottom, glides and chair casters dimensions and materials are in accordance with floor protection requirements published in Capri Mediterra 2.0 care & maintenance documents prior to Substantial Completion.

END OF SECTION