SECTION 09 51 00 – USG UMBRAL™ DIRECT MOUNT PANELS

Product Summary:

- Acoustically absorbent panels that blend in or stand out as desired - Easy to install direct to deck using hat channel and fasteners - Can be installed in addition to other specialty ceilings as a backdrop or alone as an acoustic treatment for open plenum design - ClimaPlus™ 30-year limited system warranty against visible sag, mold and mildew. - <insert product representative here> or 800.874.4968 for technical questions.

Note to Specifier:

- This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections: 09 51 00.

- 2.3   USG UMBRAL™ DIRECT MOUNT PANELS

        - Direct Mount Acoustical Panel Type <INSERT DESIGNATION HERE>:

Basis of Design: Subject to compliance with project requirements, the design is based on the following: USG Interiors, LLC, “USG UmbralTM Direct Mount Panels”.

Classification:  Provide ceiling panels complying with ASTM E 1264 for type, form and pattern as follows:

Type: IV, mineral base with membrane faced overlay

Form: 1 & 2, Nodular and water felted

Pattern: E & G, smooth and light texture

Surface Burning ASTM E84:

Material Classification: Class A

Flame Spread: 25 or less

Smoke Developed: 50 or less

Color: Manufacturer’s standard [Flat White 050] [Flat Black 205] [Field Finish 099 – Airless Spray Paint].

LR: Not less than 0.90 (only on flat white).

NRC: Not less than 0.75.

Edge/Joint Detail: SQ Square.

Mounting: [D-20 ¾” (19 mm) furring strip] [Direct Mount 7/8” (22 mm) Hat Channel]  [Direct Mount 1 ½” (38 mm) Hat Channel].

Panel Thickness: 3/4 inch (19 mm).

Nominal Modular Size: 24 by 48 inches (610 by 1220 mm).

Recycled Content: 68%.

ClimaPlus™ 30 year warranty performance: Contains a broad spectrum antimicrobial additive on the face and back of the panel that provides resistance against the growth of mold and mildew.  Includes sag resistance performance.

- END OF SECTION

Disclaimer:  The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The Specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project.  These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic text files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications and Drawings is the sole responsibility of the Design Professional.