SECTION 09 65 00 – RESILIENT FLOORING EPDM RUBBER & CORK GENERAL

  - SUMMARY

    - SECTION INCLUDES:

      - Recycled rubber cork

      - Recycled rubber cork / Recycled rubber square-edge tile

      - Adhesives

      - Finishes

    - RELATED SECTIONS

      - Section 03300 - Cast-In-Place Concrete Floor substrate requirements.

      - Section 06200 - Rough Carpentry:  Floor substrate requirements.

  - REFERENCES

    - American Concrete Institute (ACI):

      - ACI 302.2R - Guide for Concrete Slabs that Receive Moisture-Sensitive Flooring Materials

    - American Society for Testing and Materials (ASTM):

      - ASTM D883 – Standard Terminology Relating to Plastics.

      - ASTM D1566 - Standard Terminology Relating to Rubber.

      - ASTM D2047 - Standard Test Method for Static Coefficient of Friction of Polish-Coated Flooring Surfaces as Measured by the James Machine.

      - ASTM D2240 - Standard Test Method for Rubber Property Durometer Hardness.

      - ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

      - ASTM E90 – Standard Test Method for Laboratory Measurement of Airborne Sound Transmission Loss of Building Partitions and Elements.

      - ASTM E413 - Classification for Rating Sound Insulation (STC).

      - ASTM E492 – Standard Test Method for Laboratory Measurement of Impact Sound Transmission Through Floor-Ceiling Assemblies Using the Tapping Machine

      - ASTM E648 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

      - ASTM E662 - Standard Test Method for Specific Optical Density of Smoke Generated by Solid Materials.

      - ASTM E989 - Standard Classification for Determination of Impact Insulation Class (IIC).

      - ASTM F137 - Standard Test Method for Flexibility of Resilient Flooring Materials with Cylindrical Mandrel Apparatus.

      - ASTM F141 - Standard Terminology Relating to Resilient Floor Coverings.

      - ASTM F376 – Standard Test Method for Thickness of Resilient Flooring Materials Having Flat Surfaces.

      - ASTM F710 - Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring.

      - ASTM F925 - Standard Test Method for Resistance to Chemicals of Resilient Flooring.

      - ASTM F970 - Standard Test Method for Static Load Limit.

      - ASTM F1514 - Standard Test Method for Measuring Heat Stability of Resilient Flooring by Color Change.

      - ASTM F1869 - Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride.

      - ASTM F1914 - Standard Test Methods for Short-Term Indentation and Residual Indentation of Resilient Floor Covering.

      - ASTM F2055 – Standard Test Method for Size and Squareness of Resilient Floor Tile.

      - ASTM F2199 - Standard Test Method for Determining Dimensional Stability of Resilient Floor Tile after Exposure to Heat.

      - ASTM F2419 – Standard Practice for Installation of Thick Poured Concrete Underlayments and Preparation of the Surface to Receive Resilient Flooring.

      - ASTM F2471 – Standard Practice for Installation of Thick Poured Lightweight Cellular Concrete Underlayments and Preparation of the Surface to Receive Resilient Flooring.

    - State of California (CA)

      - CA Section 01350 – Special Environmental Requirements (Indoor Air Quality)

    - California Department of Public Health (CDPH)

      - CDPH Standard Method v 1.2 - Standard Method for Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers

    - California High Performance Schools (CHPS)

      - CHPS Section 01350 - Low-Emitting Materials Criteria for Use in Classrooms.

    - Declare™

      - Product material disclosure labeling program.

    - FloorScore®

      - Indoor Air Quality (IAQ) certification for flooring materials, adhesives and underlayments.

    - Living Building Challenge (LBC)

      - LBC Chemical Red List Version 3.0.

    - National Fire Protection Association (NFPA)

      - NFPA 80 – Fire Safety Code.

      - NFPA 253 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

      - NFPA 255 - Standard Test Method for Surface Burning Characteristics of Building Materials.

      - NFPA 286 - Standard Methods of Fire Tests for Evaluating Contribution of Wall and Ceiling Interior Finish to Room Fire Growth.

    - Resilient Floor Covering Institute (RFCI)

      - Recommended Work Practices for Removal of Resilient Floor Coverings

  - SUBMITTALS

    - General: Submittals must be submitted the under provisions of Section 01300.

    - Product Data:  Manufacturer's published documents on each product to be used, including:

      - Storage and handling requirements.

      - Installation instructions and initial maintenance instructions per Technical Data Sheets.

      - Maintenance and initial finish application instructions per Care & Maintenance documents.

    - Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

    - Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (150 mm) square or one full tile, representing actual product, color, and patterns.

  - SUSTAINABILITY REQUIREMENTS

    - CA Section 01350 / CHPS Section 01350

        - Provide building materials that comply with CA Section 01350 and CHPS Section 01350 when tested in accordance with CDPH Standard Method v 1.2.

        - Provide test data or third party certification that confirms compliance, such as FloorScore certification.

    - LBC Chemical Red List 3.0

        - Provide building materials that are Red List Free in accordance the LBC Chemical Red List 3.0.

        - Provide full material disclosure or third party certification that confirms compliance, such as Declare labeling.

  - QUALITY ASSURANCE

    - Qualifications:

      - Installer Qualifications: Installer must be a professional, licensed and experienced installer. Installer must have familiarity with both the type, size and format of the product.

      - Manufacturer’s Qualifications: Manufacturer must provide remote and field technical support and service prior to, during and following installation, as necessary.

    - Mock-Up:

        - Provide a mock-up for evaluation of product, surface preparation techniques and installation workmanship.

        - Do not proceed with remaining work until size, color, thickness, sheen and workmanship are approved by Architect, End-User and/or other stakeholders.

        - Maintain mock-up area as required in accordance with Care & Maintenance documents to produce acceptable work.

  - DELIVERY HANDLING & STORAGE

    - Ordering: Comply with manufacturer’s ordering and lead time requirements to avoid construction delays.

    - Storage: Store products in climate controlled space (65° F (19° C) - 85° F (30° C)) for at least 48 hours prior to installation. Keep products in manufacturer's unopened packaging until ready for installation (except for rolled goods).

    - Acclimation: Rolled goods must be unrolled and allowed to relax and acclimate for 24 hours prior to installation.

  - PROJECT CONDITIONS

      - Environmental Conditions: Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer in accordance with product technical data sheets.  Do not install products under environmental conditions outside manufacturer's absolute limits.

    - WARRANTY

      - Project Warranty: Refer to Conditions of Contract for project warranty provisions.

      - Manufacturer’s Commercial Warranty: AND/OR 2.0 Rubber Cork shall be warranted for ten years for material or manufacture defects.

- PRODUCTS

  - PRODUCT MANUFACTURERS

    - Acceptable Manufacturer:

      - Capri Collections

215 Bucky Drive

Lititz, PA  17543

P: 800.492.2613 
E: sales@capricollections.com

Web: www.capricollections.com

  - SUBSTITUTIONS

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 01 section on product options and substitutions.

    - Substitutions:  Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Division 01.

  - PRODUCT DIMENSIONS

    - Product: Capri AND/OR 2.0 Rubber Cork rolled goods, square-edge tile as manufactured by Capri Collections.

    - Square-Edge Tile Sizes (all sizes nominal):

    - ** NOTE TO SPECIFIER ** Delete sizes not required.

      - 24 inches by 24 inches by 1/8 inches (610 mm by 610 mm by 3.2 mm) Incremental minimums will apply.

      - 24 inches by 24 inches by 5/16 inches (610 mm by 610 mm by 8 mm) Incremental minimums will apply.

    - Rolled goods sizes (all sizes nominal):

** NOTE TO SPECIFIER ** Delete sizes not required. Adjust length based on desired cut, no less than 25 feet.

      - 4 feet by 25’feet by 1/8 inches (1 m by 24 m by 3.2 mm)

      - 4 feet by 25’ feet by 5/16 inches (1 m by 10.5 m by 8 mm) Incremental minimums will apply.

  - PRODUCT COLOR

** NOTE TO SPECIFIER ** Delete colors not required.

- AND/OR Rubber Cork

  - Alabaster AD4000

  - Limestone AD4001

  - Nickel AD4002

  - Linen AD4003

  - Rye AD4004

  - Reed AD4005

  - Canvas AD4006

  - Straw AD4007

  - Flax AD4008

  - Raffia AD4009

  - Carob AD4010

  - Onyx AD4011

  - Goldenrod AD4012

  - Persimmon AD4013

  - Pomegranate AD4014

  - Amethyst AD4015

  - Lapis AD4016

  - Sapphire AD4017

  - Malachite AD4018

  - PHYSICAL CHARACTERISTICS

    - ASTM F137 – Flexibility: Passes

    - ASTM F970 – Static Load Limit: Passes, 250 lbs.

    - ASTM F2199 – Dimensional Stability: Passes, <0.05 in. change

    - ASTM F1514 – Color Heat Stability: Passes, ΔE<8

    - ASTM F925 – Chemical Resistance:

      - White vinegar (5% Acetic Acid) - Passes.

      - Rubbing Alcohol (70% Isopropyl Alcohol) - Passes.

      - Lye (5% Sodium Hydroxide) - Passes.

      - Disinfectant Cleaner (5% Active Phenol) - Passes.

      - White Mineral Oil (medicinal grade) - Passes.

      - Household Bleach (5.25% NaOCl) - Passes.

      - Unleaded Gasoline - Passes.

      - Kerosene – Passes.

    - ASTM D2240 – Hardness: 85, Shore A

    - ASTM E648 (NFPA 253) – Critical Radiant Flux: Class I, > 0.45 W/cm2

    - ASTM E662 (NFPA 258) – Smoke Density: Passes, <450

    - ASTM E84 (NFPA 286) – Flammability: Class C, 76 - 200

    - ASTM D2047 – Slip Resistance: >0.8 (wet), >0.8 (dry)

    - ASTM E492/E989 – Impact Sound Transmission – 6” Concrete, Drop Ceiling: IIC 56

    - ASTM E90/E413 – Airborne Sound Transmission – 6” Concrete, Drop Ceiling: STC 54

  - PRODUCT FINISH

** NOTE TO SPECIFIER ** Finish is not optional when installed horizontally / as a floor.

    - Only Capri Collections approved floor finishes shall be used when installing AND/OR 2.0 Rubber Cork.

      - Site-Applied Urethane Finish: Loba 2K InvisibleProtect.

      - Site-Applied Urethane Finish: Loba Supra AT Satin.

    - Only Capri Collections approved floor finishes shall be used when installing AND/OR 2.0 Rubber Cork.

      - Site-Applied Acrylic Finish: Hilway Direct Plus Matte. Vertical only.

      - Site-Applied Acrylic Finish: Hilway Direct Plus Satin. Vertical only.

  - PRODUCT ADHESIVE

** NOTE TO SPECIFIER ** Delete adhesive not required.

    - Only Capri Collections approved adhesives shall be used when installing AND/OR 2.0 Rubber Cork.

      - Gold Series MA 2000 Modified Acrylic Spray Adhesive

      - Gold Series AA 2010 Acrylic Vertical Spray Adhesive

      - Gold Series AW 3000 Acrylic Resilient Flooring Adhesive

      - Gold Series MW 3012 Modified Silane Resilient Flooring Adhesive

- EXECUTION

** NOTE TO SPECIFIER ** Revise articles below to suit specific project requirements.

  - MANUFACTURERS INSTRUCTIONS

    - Compliance: Review and comply with manufacturer’s technical data sheets, care & maintenance documents, warranty information, technical bulletins and written specifications.

  - EXAMINATION

    - Site Verification of Conditions:

      - Verify substrate conditions, which have been previously installed under other sections, are acceptable for product installation in accordance with manufacturer’s technical data.

      - Do not begin installation until all substrates have been properly tested and prepared in accordance with Capri AND/OR 2.0 Rubber Cork technical data sheets and applicable ASTM, ACI, NWFA and RFCI standards.

      - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Cleaning: Clean surfaces thoroughly prior to installation.

    - Substrate Preparation: Prepare surfaces in accordance with substrate preparation requirements published in Capri AND/OR 2.0 Rubber Cork technical data sheets.

  - INSTALLATION

    - Flooring Installation: Install materials in accordance with installation instructions published in Capri AND/OR 2.0 Rubber technical data sheets.

    - Traffic Limits: Light foot traffic is allowed on the floor upon completion.  No cleaning, finishing or placement of furniture should not occur in accordance with traffic limits published in Capri AND/OR 2.0 Rubber Cork technical data sheets.

    - Initial Maintenance: Once adhesive has cured, perform initial maintenance in accordance with initial maintenance instructions published in Capri AND/OR 2.0 technical data sheets and care & maintenance documents.

  - FINISH APPLICATION

    - Initial Maintenance: Ensure surfaces have had initial maintenance performed in accordance with initial maintenance instructions published in Capri AND/OR 2.0 Rubber Cork technical data sheets and care & maintenance documents.

    - Cleaning: Clean surfaces thoroughly prior to installation.

    - Finish Application: Install finish in accordance with initial finish application instructions published in Capri AND/OR 2.0 Rubber Cork technical data sheets and care & maintenance documents.

  - MAINTENANCE

    - Daily Maintenance: Long-term care and maintenance must be performed in accordance with daily and routine maintenance instructions published in Capri AND/OR 2.0 Rubber Cork care & maintenance documents.

    - Finish Reapplication: Site-applied finish that is improperly applied or damaged may require finish re-application in accordance with finish removal and reapplication instructions published in Capri AND/OR 2.0 Rubber Cork care & maintenance documents.

  - PROTECTION

    - Temporary Floor Protection: Protect installed products until completion of project in accordance with flooring or material protection requirements published in Capri AND/OR 2.0 Rubber Cork technical data sheets and care & maintenance documents.

    - Repair: Touch-up, repair or replace damaged products prior to Substantial Completion.

    - Permanent Floor Protection: Ensure furniture feet/bottom, glides and chair casters dimensions and materials are in accordance with floor protection requirements published in Capri AND/OR 2.0 Rubber Cork care & maintenance documents prior to Substantial Completion.

END OF SECTION