SECTION 09 72 13 - CORK WALL COVERING

- GENERAL

  - SUMMARY

    - SECTION INCLUDES:

      - Cork wall covering

      - Adhesives

  - REFERENCES

    - American Society for Testing and Materials (ASTM):

      - ASTM C-423 - Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

      - ASTM C-518 - Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus.

      - ASTM D2047 - Standard Test Method for Static Coefficient of Friction of Polish-Coated Flooring Surfaces as Measured by the James Machine.

      - ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

      - ASTM E413 - Classification for Rating Sound Insulation.

      - ASTM F137 - Standard Test Method for Flexibility of Resilient Flooring Materials with Cylindrical Mandrel Apparatus.

      - ASTM F141 - Standard Terminology Relating to Resilient Floor Coverings

      - ASTM F386 – Standard Test Method for Thickness of Resilient Flooring Materials Having Flat Surfaces

      - ASTM F710 - Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring.

      - ASTM F925 - Standard Test Method for Resistance to Chemicals of Resilient Flooring.

      - ASTM F970 - Standard Test Method for Static Load Limit.

      - ASTM F1482 – Standard Practice for Installation and Preparation of Panel Type Underlayments to Receive Resilient Flooring.

      - ASTM F1869 - Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride

      - ASTM F1914 - Standard Test Methods for Short-Term Indentation and Residual Indentation of Resilient Floor Covering.

      - ASTM F2055 – Standard Test Method for Size and Squareness of Resilient Floor Tile

      - ASTM F2199 - Standard Test Method for Determining Dimensional Stability of Resilient Floor Tile after Exposure to Heat.

      - ASTM F3008 – Standard Specification for Cork Floor Tile

    - State of California (CA)

      - CA Section 01350 – Special Environmental Requirements (Indoor Air Quality)

    - California Department of Public Health (CDPH)

      - CDPH Standard Method v 1.2 - Standard Method for Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers

    - California High Performance Schools (CHPS)

      - CHPS Section 01350 - Low-Emitting Materials Criteria for Use in Classrooms.

    - European Committee for Standardization (CEN)

      - European Norms (EN)

        - EN 434 – Resilient Floor Coverings – Determination of Dimensional Stability and Curling after Exposure to Heat

    - International Organization for Standardization (ISO)

      - ISO 4918 – Resilient, Textile and Laminate Floor Coverings – Castor Chair Test

      - ISO 24338 – Laminate Floor Coverings – Determination of Abrasion Resistance

    - Living Building Challenge (LBC)

      - LBC Chemical Red List Version 3.0.

    - National Fire Protection Association (NFPA)

      - NFPA 80 – Fire Safety Code.

      - NFPA 253 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

      - NFPA 255 - Standard Test Method for Surface Burning Characteristics of Building Materials.

      - NFPA 286 - Standard Methods of Fire Tests for Evaluating Contribution of Wall and Ceiling Interior Finish to Room Fire Growth.

    - Resilient Floor Covering Institute (RFCI)

      - Recommended Work Practices for Removal of Resilient Floor Coverings

  - SUBMITTALS

    - General: Submittals must be submitted the under provisions of Section 01300.

    - Product Data:  Manufacturer's published documents on each product to be used, including:

      - Storage and handling requirements.

      - Installation instructions and initial maintenance instructions per Technical Data Sheets.

      - Maintenance and initial finish application instructions per Care & Maintenance documents.

    - Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

    - Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (150 mm) square or one full tile, representing actual product, color, and patterns.

  - SUSTAINABILITY REQUIREMENTS

    - CA Section 01350 / CHPS Section 01350

        - Provide building materials that comply with CA Section 01350 and CHPS Section 01350 when tested in accordance with CDPH Standard Method v 1.2.

        - Provide test data or third party certification that confirms compliance.

    - LBC Chemical Red List 3.0

        - Provide building materials that are Red List Free in accordance the LBC Chemical Red List 3.0.

        - Provide full material disclosure or third party certification that confirms compliance.

  - QUALITY ASSURANCE

    - Cork Tile

      - Cork tile is a natural product – as such, shade and color variations are inherent.

    - Qualifications:

      - Installer Qualifications: Installer must be a professional, licensed and experienced installer. Installer must have familiarity with both the type, size and format of the product.

      - Manufacturer’s Qualifications: Manufacturer must provide remote and field technical support and service prior to, during and following installation, as necessary.

    - Mock-Up:

      - Provide a mock-up for evaluation of product, surface preparation techniques and installation workmanship.

      - Do not proceed with remaining work until size, color, thickness, sheen and workmanship are approved by Architect, End-User and/or other stakeholders.

      - Maintain mock-up area as required in accordance with Care & Maintenance documents to produce acceptable work.

  - DELIVERY HANDLING & STORAGE

    - Ordering: Comply with manufacturer’s ordering and lead time requirements to avoid construction delays.

    - Storage: Store products in climate controlled space (65° F (19° C) - 85° F (30° C), 45% - 55% RH) for at least 72 hours prior to installation. Keep products in manufacturer's unopened packaging until ready for installation (except for rolled goods).

    - Acclimation: Rolled goods must be unrolled and allowed to relax and acclimate for 24 hours prior to installation.

  - PROJECT CONDITIONS

      - Environmental Conditions: Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer in accordance with product technical data sheets.  Do not install products under environmental conditions outside manufacturer's absolute limits.

    - WARRANTY

      - Project Warranty: Refer to Conditions of Contract for project warranty provisions.

      - Manufacturer’s Commercial Warranty: Muro shall be warranted for ten years for material or manufacture defects.

- PRODUCTS

  - PRODUCT MANUFACTURERS

    - Acceptable Manufacturer:

      - Capri Collections

215 Bucky Drive

Lititz, PA  17543

P: 800.492.2613 
E: sales@capricollections.com

Web: www.capricollections.com

  - SUBSTITUTIONS

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 01 section on product options and substitutions.

    - Substitutions:  Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Division 01.

  - PRODUCT DIMENSIONS

    - Product: Capri Muro Cork Wall Tile

    - Gallery Tile Sizes (all sizes nominal):

** NOTE TO SPECIFIER ** Delete sizes not required.

      - 12 inches by 24 inches by 0.11 inches (300 mm x 600 mm x 3 mm)

    - Studio Tile Sizes (all sizes nominal):

** NOTE TO SPECIFIER ** Delete sizes not required.

      - 12 inches by 24 inches by 0.15 inches (300 mm x 600 mm x 4 mm)

    - Fresh Tile Sizes (all sizes are nominal)

**NOTE TO SPECIFIER **Delete sizes not required.

      - 12 inches by 12 inches by 0.11 inches (300 mm x 300 mm x 3mm)

  - PRODUCT COLOR

    - Gallery

** NOTE TO SPECIFIER ** Delete colors not required.

      - Abstract White MWT201

      - Montage MWT202

      - Mosaic MWT203

      - Etching MWT204

      - Drawing MWT205

      - Collage MWT207

      - Sculpture MWT207

      - Abstract Black MWT208

    - Studio

** NOTE TO SPECIFIER ** Delete colors not required.

      - Art MWT101

      - Music MWT102

      - Dance MWT103

      - Design MWT104

      - Sound MWT105

      - Photography MWT106

      - Film MWT017

    - Fresh

**NOTE TO SPECIFIER ** Delete colors not required.

      - Air MWT002

      - Atmosphere MWT004

      - Pressure MWT003

      - Sky MWT006

      - Sphere MWT005

      - Stratosphere MWT001

*Patterns Stratosphere, Air, Pressure, and Atmosphere contain a single design with no variations from tiles to tile. Sphere and Sky patterns each have a number of variations.

  - PHYSICAL CHARACTERISTICS

      - EN 23999 – Curling: Passes, <6mm

      - EN – Dimensional Variation: <0.04 in. change

      - ASTM F925 – Chemical Resistance:

        - White vinegar (5% Acetic Acid) - Passes.

        - Rubbing Alcohol (70% Isopropyl Alcohol) - Passes.

        - Hydrochloric Acid (5% HCI) - Passes.

        - Household Ammonia (5% Ammonia) - Passes.

        - Disinfectant Cleaner (5% Active Phenol) - Passes.

        - Household Bleach (5.25% NaOCl) - Passes.

        - Unleaded Gasoline - Passes.

        - Kerosene - Passes.

        - Olive Oil - Passes.

        - Coffee – Passes.

    - ASTM E84 (NFPA 286) – Flammability – Gallery/Fresh: Class B, 26 - 75

    - ASTM E84 (NFPA 286) – Flammability - Studio: Class C, 76 - 200

    - EN ISO 354 – Noise Reduction: Gallery/Fresh– aw 0.05 / Studio – aw 0.10

  - PRODUCT ADHESIVE

** NOTE TO SPECIFIER ** Adhesive is not optional.

    - Only Capri Collections approved adhesives shall be used when installing Muro.

      - Gold Series WC 1000 Water-Based Cork Contact Adhesive

- EXECUTION

** NOTE TO SPECIFIER ** Revise articles below to suit specific project requirements.

  - MANUFACTURERS INSTRUCTIONS

    - Compliance: Review and comply with manufacturer’s technical data sheets, care & maintenance documents, warranty information, technical bulletins and written specifications.

  - EXAMINATION

    - Site Verification of Conditions:

      - Verify substrate conditions, which have been previously installed under other sections, are acceptable for product installation in accordance with manufacturer’s technical data.

      - Do not begin installation until all substrates have been properly tested and prepared in accordance with Capri Muro technical data sheets and applicable ASTM standards.

      - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Cleaning: Clean surfaces thoroughly prior to installation.

    - Substrate Preparation: Prepare surfaces in accordance with substrate preparation requirements published in Capri Muro technical data sheets.

  - INSTALLATION

    - Installation: Install materials in accordance with installation instructions published in Capri Muro technical data sheets.

    - Traffic Limits: No traffic, cleaning, finishing or placement of furniture should occur in accordance with adhesive traffic limits published in adhesive technical data.

    - Initial Maintenance: Once traffic limits have lapsed, perform initial maintenance in accordance with initial maintenance instructions published in Capri Muro technical data sheets and care & maintenance documents.

  - MAINTENANCE

    - Daily Maintenance: Long-term care and maintenance must be performed in accordance with daily and routine maintenance instructions published in Capri Muro care & maintenance documents.

  - PROTECTION

    - Temporary Protection: Protect installed products until completion of project in accordance with material protection requirements published in Capri Muro technical data sheets and care & maintenance documents.

    - Repair: Touch-up, repair or replace damaged products prior to Substantial Completion.

END OF SECTION